Supplementary data. Mapping Gas Permeability of Sustainable Packaging Materials to Link Food Barrier Needs by Clustering Algorithms

Ting Yu Yeh1, Deniz Turan 1*

1 Food Quality and Design, Wageningen University & Research, P.O. Box 17, 6700 AA Wageningen, the Netherlands

Supplementary Material

This supplementary document presents a comprehensive summary of the clustering analysis conducted in this study. It includes detailed results for the DBSCAN model (Supplementary Table 1 to Table 3, OTR (cm3/m2day) at 23 °C and 50% RH, and WVTR (g/m2day) at 25 °C and 50% RH for assumed thickness 100 μm) and the outcomes from the two alternative models, K-Means and Gaussian Mixture Model (GMM) are shown as supplementary Figure 1 and Figure 2. The appendix provides visualizations of the clusters. Supplementary Figure 4. K-Distance Plot for Determining DBSCAN ε Parameter. The “elbow” observed at the 245th point corresponds to an ε value of 1.17, which was selected as the optimal neighborhood radius for the DBSCAN clustering algorithm. While smaller changes in slope can be seen before the 245th point, these represent local fluctuations rather than the global “knee.” Selecting such earlier elbow points would have led to unstable clustering results, with the majority of points classified as noise and poor alignment with known material–food barrier property ranges. In contrast, ε = 1.17 yielded three stable and interpretable clusters (see Figure 3 and Table 4 in the manuscript).

Supplementary Table 1. The data points in cluster 1

| Base Material | Type | Secondary Material | OTR (cm3/m2day) | WVTR (g/m2day) |
| --- | --- | --- | --- | --- |
| fish gelatin | individual | None | 4.028 | 2,731.398 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 1.144 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 1.964 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 1.713 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 2.142 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 1.899 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 2.48 | 1,208.118 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 709.113 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 980.502 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,199.364 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,365.699 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,085.556 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,076.801 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,146.837 |
| fish gelatin | nanocomposite | montmorillonite | 2.073 | 1,208.118 |

Supplementary Table 2. The data points in cluster 2

| Base Material | Type | Secondary Material | OTR (cm3/m2day) | WVTR (g/m2day) |
| --- | --- | --- | --- | --- |
| LDPE | individual | None | 18,948.197 | 114.438 |
| LDPE | individual | None | 18,948.197 | 76.164 |
| HDPE | individual | None | 4,326.464 | 19.26 |
| polylactic acid | individual | None | 711.302 | 2,203.925 |
| polylactic acid | individual | None | 711.302 | 1,904.099 |
| polylactic acid | individual | None | 711.302 | 4,463.444 |
| polylactic acid | individual | None | 10,681.596 | 2,203.925 |
| polylactic acid | individual | None | 10,681.596 | 1,904.099 |
| polylactic acid | individual | None | 10,681.596 | 4,463.444 |
| polylactic acid | individual | None | 171.238 | 2,203.925 |
| polylactic acid | individual | None | 171.238 | 1,904.099 |
| polylactic acid | individual | None | 171.238 | 4,463.444 |

Supplementary Table 3. The data points in cluster 3

| Base Material | Type | Secondary Material | OTR (cm3/m2day) | WVTR (g/m2day) |
| --- | --- | --- | --- | --- |
| carrot puree | blend | CMC | 17.745 | 580,509.569 |
| carrot puree | blend | CMC | 17.745 | 427,743.893 |
| carrot puree | blend | CMC | 17.745 | 248,977.411 |
| carrot puree | blend | CMC | 17.745 | 202,053.398 |
| carrot puree | blend | CMC | 17.745 | 185,770.066 |
| carrot puree | blend | CMC | 17.745 | 154,166.393 |
| carrot puree | blend | CMC | 17.745 | 286,446.586 |
| carrot puree | blend | CMC | 17.745 | 276,028.754 |
| carrot puree | blend | CMC | 17.745 | 235,407.967 |
| carrot puree | blend | CMC | 17.745 | 213,784.402 |
| carrot puree | blend | CMC | 17.745 | 200,127.413 |
| carrot puree | blend | CMC | 17.745 | 190,935.209 |
| carrot puree | blend | CMC | 15.828 | 580,509.569 |
| carrot puree | blend | CMC | 15.828 | 427,743.893 |
| carrot puree | blend | CMC | 15.828 | 248,977.411 |
| carrot puree | blend | CMC | 15.828 | 202,053.398 |
| carrot puree | blend | CMC | 15.828 | 185,770.066 |
| carrot puree | blend | CMC | 15.828 | 154,166.393 |
| carrot puree | blend | CMC | 15.828 | 286,446.586 |
| carrot puree | blend | CMC | 15.828 | 276,028.754 |
| carrot puree | blend | CMC | 15.828 | 235,407.967 |
| carrot puree | blend | CMC | 15.828 | 213,784.402 |
| carrot puree | blend | CMC | 15.828 | 200,127.413 |
| carrot puree | blend | CMC | 15.828 | 190,935.209 |
| carrot puree | blend | CMC | 13.009 | 580,509.569 |
| carrot puree | blend | CMC | 13.009 | 427,743.893 |
| carrot puree | blend | CMC | 13.009 | 248,977.411 |
| carrot puree | blend | CMC | 13.009 | 202,053.398 |
| carrot puree | blend | CMC | 13.009 | 185,770.066 |
| carrot puree | blend | CMC | 13.009 | 154,166.393 |
| carrot puree | blend | CMC | 13.009 | 286,446.586 |
| carrot puree | blend | CMC | 13.009 | 276,028.754 |
| carrot puree | blend | CMC | 13.009 | 235,407.967 |
| carrot puree | blend | CMC | 13.009 | 213,784.402 |
| carrot puree | blend | CMC | 13.009 | 200,127.413 |
| carrot puree | blend | CMC | 13.009 | 190,935.209 |
| carrot puree | blend | CMC | 12.037 | 580,509.569 |
| carrot puree | blend | CMC | 12.037 | 427,743.893 |
| carrot puree | blend | CMC | 12.037 | 248,977.411 |
| carrot puree | blend | CMC | 12.037 | 202,053.398 |
| carrot puree | blend | CMC | 12.037 | 185,770.066 |
| carrot puree | blend | CMC | 12.037 | 154,166.393 |
| carrot puree | blend | CMC | 12.037 | 286,446.586 |
| carrot puree | blend | CMC | 12.037 | 276,028.754 |
| carrot puree | blend | CMC | 12.037 | 235,407.967 |
| carrot puree | blend | CMC | 12.037 | 213,784.402 |
| carrot puree | blend | CMC | 12.037 | 200,127.413 |
| carrot puree | blend | CMC | 12.037 | 190,935.209 |
| carrot puree | blend | CMC | 11.442 | 580,509.569 |
| carrot puree | blend | CMC | 11.442 | 427,743.893 |
| carrot puree | blend | CMC | 11.442 | 248,977.411 |
| carrot puree | blend | CMC | 11.442 | 202,053.398 |
| carrot puree | blend | CMC | 11.442 | 185,770.066 |
| carrot puree | blend | CMC | 11.442 | 154,166.393 |
| carrot puree | blend | CMC | 11.442 | 286,446.586 |
| carrot puree | blend | CMC | 11.442 | 276,028.754 |
| carrot puree | blend | CMC | 11.442 | 235,407.967 |
| carrot puree | blend | CMC | 11.442 | 213,784.402 |
| carrot puree | blend | CMC | 11.442 | 200,127.413 |
| carrot puree | blend | CMC | 11.442 | 190,935.209 |
| carrot puree | blend | CMC | 11.004 | 580,509.569 |
| carrot puree | blend | CMC | 11.004 | 427,743.893 |
| carrot puree | blend | CMC | 11.004 | 248,977.411 |
| carrot puree | blend | CMC | 11.004 | 202,053.398 |
| carrot puree | blend | CMC | 11.004 | 185,770.066 |
| carrot puree | blend | CMC | 11.004 | 154,166.393 |
| carrot puree | blend | CMC | 11.004 | 286,446.586 |
| carrot puree | blend | CMC | 11.004 | 276,028.754 |
| carrot puree | blend | CMC | 11.004 | 235,407.967 |
| carrot puree | blend | CMC | 11.004 | 213,784.402 |
| carrot puree | blend | CMC | 11.004 | 200,127.413 |
| carrot puree | blend | CMC | 11.004 | 190,935.209 |
| carrot puree | blend | CMC | 11.897 | 580,509.569 |
| carrot puree | blend | CMC | 11.897 | 427,743.893 |
| carrot puree | blend | CMC | 11.897 | 248,977.411 |
| carrot puree | blend | CMC | 11.897 | 202,053.398 |
| carrot puree | blend | CMC | 11.897 | 185,770.066 |
| carrot puree | blend | CMC | 11.897 | 154,166.393 |
| carrot puree | blend | CMC | 11.897 | 286,446.586 |
| carrot puree | blend | CMC | 11.897 | 276,028.754 |
| carrot puree | blend | CMC | 11.897 | 235,407.967 |
| carrot puree | blend | CMC | 11.897 | 213,784.402 |
| carrot puree | blend | CMC | 11.897 | 200,127.413 |
| carrot puree | blend | CMC | 11.897 | 190,935.209 |
| carrot puree | blend | CMC | 12.02 | 580,509.569 |
| carrot puree | blend | CMC | 12.02 | 427,743.893 |
| carrot puree | blend | CMC | 12.02 | 248,977.411 |
| carrot puree | blend | CMC | 12.02 | 202,053.398 |
| carrot puree | blend | CMC | 12.02 | 185,770.066 |
| carrot puree | blend | CMC | 12.02 | 154,166.393 |
| carrot puree | blend | CMC | 12.02 | 286,446.586 |
| carrot puree | blend | CMC | 12.02 | 276,028.754 |
| carrot puree | blend | CMC | 12.02 | 235,407.967 |
| carrot puree | blend | CMC | 12.02 | 213,784.402 |
| carrot puree | blend | CMC | 12.02 | 200,127.413 |
| carrot puree | blend | CMC | 12.02 | 190,935.209 |
| carrot puree | blend | CMC | 12.046 | 580,509.569 |
| carrot puree | blend | CMC | 12.046 | 427,743.893 |
| carrot puree | blend | CMC | 12.046 | 248,977.411 |
| carrot puree | blend | CMC | 12.046 | 202,053.398 |
| carrot puree | blend | CMC | 12.046 | 185,770.066 |
| carrot puree | blend | CMC | 12.046 | 154,166.393 |
| carrot puree | blend | CMC | 12.046 | 286,446.586 |
| carrot puree | blend | CMC | 12.046 | 276,028.754 |
| carrot puree | blend | CMC | 12.046 | 235,407.967 |
| carrot puree | blend | CMC | 12.046 | 213,784.402 |
| carrot puree | blend | CMC | 12.046 | 200,127.413 |
| carrot puree | blend | CMC | 12.046 | 190,935.209 |
| carrot puree | blend | CMC | 12.239 | 580,509.569 |
| carrot puree | blend | CMC | 12.239 | 427,743.893 |
| carrot puree | blend | CMC | 12.239 | 248,977.411 |
| carrot puree | blend | CMC | 12.239 | 202,053.398 |
| carrot puree | blend | CMC | 12.239 | 185,770.066 |
| carrot puree | blend | CMC | 12.239 | 154,166.393 |
| carrot puree | blend | CMC | 12.239 | 286,446.586 |
| carrot puree | blend | CMC | 12.239 | 276,028.754 |
| carrot puree | blend | CMC | 12.239 | 235,407.967 |
| carrot puree | blend | CMC | 12.239 | 213,784.402 |
| carrot puree | blend | CMC | 12.239 | 200,127.413 |
| carrot puree | blend | CMC | 12.239 | 190,935.209 |
| carrot puree | blend | CMC | 12.475 | 580,509.569 |
| carrot puree | blend | CMC | 12.475 | 427,743.893 |
| carrot puree | blend | CMC | 12.475 | 248,977.411 |
| carrot puree | blend | CMC | 12.475 | 202,053.398 |
| carrot puree | blend | CMC | 12.475 | 185,770.066 |
| carrot puree | blend | CMC | 12.475 | 154,166.393 |
| carrot puree | blend | CMC | 12.475 | 286,446.586 |
| carrot puree | blend | CMC | 12.475 | 276,028.754 |
| carrot puree | blend | CMC | 12.475 | 235,407.967 |
| carrot puree | blend | CMC | 12.475 | 213,784.402 |
| carrot puree | blend | CMC | 12.475 | 200,127.413 |
| carrot puree | blend | CMC | 12.475 | 190,935.209 |
| carrot puree | blend | CMC | 12.72 | 580,509.569 |
| carrot puree | blend | CMC | 12.72 | 427,743.893 |
| carrot puree | blend | CMC | 12.72 | 248,977.411 |
| carrot puree | blend | CMC | 12.72 | 202,053.398 |
| carrot puree | blend | CMC | 12.72 | 185,770.066 |
| carrot puree | blend | CMC | 12.72 | 154,166.393 |
| carrot puree | blend | CMC | 12.72 | 286,446.586 |
| carrot puree | blend | CMC | 12.72 | 276,028.754 |
| carrot puree | blend | CMC | 12.72 | 235,407.967 |
| carrot puree | blend | CMC | 12.72 | 213,784.402 |
| carrot puree | blend | CMC | 12.72 | 200,127.413 |
| carrot puree | blend | CMC | 12.72 | 190,935.209 |
| carrot puree | blend | gelatin | 12.09 | 251,428.666 |
| carrot puree | blend | gelatin | 12.09 | 211,333.147 |
| carrot puree | blend | gelatin | 12.09 | 188,746.589 |
| carrot puree | blend | gelatin | 12.09 | 237,333.953 |
| carrot puree | blend | gelatin | 12.09 | 303,692.911 |
| carrot puree | blend | gelatin | 12.09 | 335,121.494 |
| carrot puree | blend | gelatin | 11.355 | 251,428.666 |
| carrot puree | blend | gelatin | 11.355 | 211,333.147 |
| carrot puree | blend | gelatin | 11.355 | 188,746.589 |
| carrot puree | blend | gelatin | 11.355 | 237,333.953 |
| carrot puree | blend | gelatin | 11.355 | 303,692.911 |
| carrot puree | blend | gelatin | 11.355 | 335,121.494 |
| carrot puree | blend | gelatin | 12.23 | 251,428.666 |
| carrot puree | blend | gelatin | 12.23 | 211,333.147 |
| carrot puree | blend | gelatin | 12.23 | 188,746.589 |
| carrot puree | blend | gelatin | 12.23 | 237,333.953 |
| carrot puree | blend | gelatin | 12.23 | 303,692.911 |
| carrot puree | blend | gelatin | 12.23 | 335,121.494 |
| carrot puree | blend | gelatin | 11.713 | 251,428.666 |
| carrot puree | blend | gelatin | 11.713 | 211,333.147 |
| carrot puree | blend | gelatin | 11.713 | 188,746.589 |
| carrot puree | blend | gelatin | 11.713 | 237,333.953 |
| carrot puree | blend | gelatin | 11.713 | 303,692.911 |
| carrot puree | blend | gelatin | 11.713 | 335,121.494 |
| carrot puree | blend | gelatin | 12.957 | 251,428.666 |
| carrot puree | blend | gelatin | 12.957 | 211,333.147 |
| carrot puree | blend | gelatin | 12.957 | 188,746.589 |
| carrot puree | blend | gelatin | 12.957 | 237,333.953 |
| carrot puree | blend | gelatin | 12.957 | 303,692.911 |
| carrot puree | blend | gelatin | 12.957 | 335,121.494 |
| carrot puree | blend | gelatin | 12.755 | 251,428.666 |
| carrot puree | blend | gelatin | 12.755 | 211,333.147 |
| carrot puree | blend | gelatin | 12.755 | 188,746.589 |
| carrot puree | blend | gelatin | 12.755 | 237,333.953 |
| carrot puree | blend | gelatin | 12.755 | 303,692.911 |
| carrot puree | blend | gelatin | 12.755 | 335,121.494 |

Supplementary Table 4. Raw data in file “semi-processed_2.csv” ,Doc,OP_Updated_Num,OP_Unit,OTR_Updated_Num,OTR_Unit,PCO2_Updated_Num,PCO2_Unit,WVTR_Updated_Num,WVTR_Unit,WVP_Updated_Num,WVP_Unit,thickness_Updated_Num,thickness_Unit,temperature_Updated_Num,temperature_Unit,RH_Updated_Num,RH_Unit,Base Material,Type,Secondary Material,Composition,Plasticizer

0,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,3.12E-11,gm/m2Pas,1E-04,,,,,,fish gelatin,individual,None,,"[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

1,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,8.1E-12,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.09â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

2,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.12E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

3,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.37E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

4,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.56E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,,glycerol

5,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.24E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,,glycerol

6,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",4.60107282214363E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,individual,None,,"[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

7,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",1.30675951055917E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.09â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

8,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",2.24342279609983E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,,glycerol

9,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",1.95671244894043E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,,glycerol

10,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",2.44674726540012E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

11,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",2.16917509663624E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

12,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",2.83283530261078E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,,glycerol

13,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",2.36793047673877E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,fish gelatin,nanocomposite,montmorillonite,,glycerol

14,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.23E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

15,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.31E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

16,"Effect of clay content, homogenization RPM, pH, and ultrasonication on mechanical and barrier properties of fish gelatin montmorillonite nanocomposite films",,,,,,,,,1.38E-11,gm/m2Pas,,,,,,,fish gelatin,nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.05â€™, â€™%â€™]","[â€˜GLYâ€™, â€™20.0â€™, â€˜%â€™]"

17,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,1.8E-11,gm/m2Pas,7.15E-05,m,25.0,Â°C,50.0,%,polylactic acid,individual,None,,

18,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,2.08E-11,gm/m2Pas,8.06E-05,m,25.0,Â°C,50.0,%,polylactic acid,nanocomposite,NaMMT,"[â€˜NaMMTâ€™, â€™0.5â€™, â€™%â€™]",

19,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,1.7E-11,gm/m2Pas,7.92E-05,m,25.0,Â°C,50.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€™0.5â€™, â€™%â€™]",

20,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,1.15E-11,gm/m2Pas,8.41E-05,m,25.0,Â°C,50.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€™0.5â€™, â€™%â€™]",

21,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,2.61E-11,gm/m2Pas,0.00012,m,25.0,Â°C,50.0,%,polylactic acid,individual,None,,

22,"Tensile, water vapor barrier and antimicrobial properties of PLA nanoclay composite films",,,,,,,,,4.66E-11,gm/m2Pas,9.14E-05,m,25.0,Â°C,50.0,%,polylactic acid,individual,None,,

23,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,6.119E-14,gm/m2Pas,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.0â€™, â€˜%â€™]"

24,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,4.313E-14,gm/m2Pas,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.0â€™, â€˜%â€™]"

25,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,4.785E-14,gm/m2Pas,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜0.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.0â€™, â€˜%â€™]"

26,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,6.25E-11,gm/m2Pas,3E-06,m,20.0,Â°C,0.0,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜0.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

27,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,6.47E-11,gm/m2Pas,3E-06,m,20.0,Â°C,0.0,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

28,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,6.18E-11,gm/m2Pas,3E-06,m,20.0,Â°C,0.0,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

29,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,1.8E-11,gm/m2Pas,3E-06,m,20.0,Â°C,,%,locust bean gum,individual,None,"[â€˜LBGâ€™, â€˜1.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€˜1.7â€™, â€˜%â€™]"

30,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,3.2E-11,gm/m2Pas,3E-06,m,20.0,Â°C,,%,locust bean gum,individual,None,"[â€˜LBGâ€™, â€˜1.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€˜0.4â€™, â€˜%â€™]"

31,Suitability of novel galactomannans as edible coatings for tropical fruits,,,,,,,,,8.7E-11,gm/m2Pas,3E-06,m,20.0,Â°C,,%,corn starch,individual,None,"[â€˜CSâ€™, â€˜5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.4â€™, â€˜%â€™]"

32,Suitability of novel galactomannans as edible coatings for tropical fruits,9.9E-16,gm/m2Pas,,,,,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜0.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

33,Suitability of novel galactomannans as edible coatings for tropical fruits,4.3E-16,gm/m2Pas,,,,,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

34,Suitability of novel galactomannans as edible coatings for tropical fruits,4.1E-16,gm/m2Pas,,,,,,,,,3E-06,m,20.0,Â°C,,%,fruit,coated,galactomannans,"[â€˜GALâ€™, â€˜1.5â€™, â€™%â€™]","[â€˜GLYâ€™, â€˜1.5â€™, â€˜%â€™]"

35,Gas transport properties of polypropylene clay composite membranes,1.95016576408995E-09,cm3cm/m2Pas,,,,,,,,,0.0001099999999999,m,25.0,Â°C,,,polypropylene,individual,None,,

36,Gas transport properties of polypropylene clay composite membranes,4.48538125740689E-10,cm3cm/m2Pas,,,,,,,,,0.000127,m,25.0,Â°C,,,polypropylene,nanocomposite,NaMMT,"[â€˜NaMMTâ€™, â€™5.0â€™, â€™%â€™]",

37,Exploring the potentialities of using lignocellulosic fibres derived from three food by-products as constituents of biocomposites for food packaging,,,,,,,,,1.5E-11,gm/m2Pas,0.00025,m,20.0,Â°C,100,%,PHBV,individual,None,,

38,Exploring the potentialities of using lignocellulosic fibres derived from three food by-products as constituents of biocomposites for food packaging,,,,,,,,,5.2E-11,gm/m2Pas,0.00025,m,20.0,Â°C,100,%,PHBV,blend,wheat straw fibres,"[â€˜WSFâ€™, â€™20.0â€™, â€™%â€™]",

39,Exploring the potentialities of using lignocellulosic fibres derived from three food by-products as constituents of biocomposites for food packaging,,,,,,,,,5.2E-12,gm/m2Pas,0.00025,m,20.0,Â°C,100,%,PHBV,blend,olive mills,"[â€˜OMâ€™, â€™20.0â€™, â€™%â€™]",

40,Barrier properties of chitosan coated polyethylene,,,,,1.02E-17,gm/m2Pas,,,,,,,25.0,Â°C,0.0,%,polyethylene,coated,chitosan,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",

41,Barrier properties of chitosan coated polyethylene,,,,,,,,,7.1E-13,gm/m2Pas,,,,,,,polyvinyl chloride,individual,None,,

42,Barrier properties of chitosan coated polyethylene,,,,,,,,,6.5E-13,gm/m2Pas,,,,,,,polypropylene,individual,None,,

43,Barrier properties of chitosan coated polyethylene,,,,,,,,,6.11E-11,gm/m2Pas,,,25.0,Â°C,50.0,%,chitosan,individual,None,,

44,Barrier properties of chitosan coated polyethylene,,,,,,,,,1.492E-12,gm/m2Pas,,,25.0,Â°C,50.0,%,chitosan,individual,None,,

45,Barrier properties of chitosan coated polyethylene,,,,,,,,,5E-11,gm/m2Pas,,,25.0,Â°C,52.0,%,methylcellulose,individual,None,,PEG

46,Barrier properties of chitosan coated polyethylene,,,,,,,,,2.2E-11,gm/m2Pas,,,,,,,oat starch,individual,None,,PEG

47,Barrier properties of chitosan coated polyethylene,,,,,,,,,4.2E-12,gm/m2Pas,,,,,,,oat starch,individual,None,,PEG

48,Barrier properties of chitosan coated polyethylene,,,,,,,,,7E-10,gm/m2Pas,0.0004,m,21.0,Â°C,85.0,%,wheat gluten,individual,None,,

49,Barrier properties of chitosan coated polyethylene,,,,,,,,,3.8E-10,gm/m2Pas,2.9E-05,m,25.0,Â°C,52.0,%,amylose,individual,None,,

50,Barrier properties of chitosan coated polyethylene,,,,,,,,,3.48E-10,gm/m2Pas,4.5E-05,m,25.0,Â°C,70.0,%,polyethylene,individual,None,,

51,Barrier properties of chitosan coated polyethylene,6.18E-17,gm/m2Pas,,,,,,,,,5E-05,m,25.0,Â°C,0.0,%,polyethylene,coated,chitosan,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",

52,Barrier properties of chitosan coated polyethylene,514.0,gm/m2Pas,,,,,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,,

53,Barrier properties of chitosan coated polyethylene,1.32,gm/m2Pas,,,,,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,,

54,Barrier properties of chitosan coated polyethylene,1.04E-17,gm/m2Pas,,,,,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,,

55,Barrier properties of chitosan coated polyethylene,4.332E-16,gm/m2Pas,,,,,,,,,,,25.0,Â°C,96.0,%,chitosan,individual,None,,

56,Barrier properties of chitosan coated polyethylene,8.76E-17,gm/m2Pas,,,,,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]","[â€˜GLYâ€™, â€™23.0â€™, â€˜%â€™]"

57,Barrier properties of chitosan coated polyethylene,1.5013E-15,gm/m2Pas,,,,,,,,,,,25.0,Â°C,96.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]","[â€˜GLYâ€™, â€™23.0â€™, â€˜%â€™]"

58,Barrier properties of chitosan coated polyethylene,,,,,6.98E-17,gm/m2Pas,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,,

59,Barrier properties of chitosan coated polyethylene,,,,,7.8E-17,gm/m2Pas,,,,,,,25.0,Â°C,96.0,%,chitosan,individual,None,,

60,Barrier properties of chitosan coated polyethylene,,,,,3.82E-16,gm/m2Pas,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]","[â€˜GLYâ€™, â€™23.0â€™, â€˜%â€™]"

61,Barrier properties of chitosan coated polyethylene,,,,,2.664E-15,gm/m2Pas,,,,,,,25.0,Â°C,96.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]","[â€˜GLYâ€™, â€™23.0â€™, â€˜%â€™]"

62,Barrier properties of chitosan coated polyethylene,,,,,,,,,5E-13,gm/m2Pas,,,25.0,Â°C,45.0,%,polyethylene,individual,None,,

63,Barrier properties of chitosan coated polyethylene,,,,,,,,,7.72E-13,gm/m2Pas,4.5E-05,m,25.0,Â°C,33.0,%,polyethylene,individual,None,,

64,Barrier properties of chitosan coated polyethylene,,,,,,,,,5.55E-13,gm/m2Pas,4.5E-05,m,25.0,Â°C,45.0,%,polyethylene,individual,None,,

65,Barrier properties of chitosan coated polyethylene,,,,,,,,,4.62E-13,gm/m2Pas,4.5E-05,m,25.0,Â°C,70.0,%,polyethylene,individual,None,,

66,Barrier properties of chitosan coated polyethylene,,,,,,,,,2.571E-12,gm/m2Pas,,,25.0,Â°C,33.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",

67,Barrier properties of chitosan coated polyethylene,,,,,,,,,2.2E-10,gm/m2Pas,,,25.0,Â°C,45.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",

68,Barrier properties of chitosan coated polyethylene,,,,,,,,,4.161E-10,gm/m2Pas,,,25.0,Â°C,70.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",

69,Barrier properties of chitosan coated polyethylene,,,,,,,,,2.614E-12,gm/m2Pas,,,25.0,Â°C,33.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

70,Barrier properties of chitosan coated polyethylene,,,,,,,,,1.905E-10,gm/m2Pas,,,25.0,Â°C,45.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

71,Barrier properties of chitosan coated polyethylene,,,,,,,,,5.41E-10,gm/m2Pas,,,25.0,Â°C,70.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

72,Barrier properties of chitosan coated polyethylene,,,,,,,,,7.88E-13,gm/m2Pas,5E-05,m,25.0,Â°C,33.0,%,polyethylene,coated,chitosan,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

73,Barrier properties of chitosan coated polyethylene,,,,,,,,,6.67E-13,gm/m2Pas,5E-05,m,25.0,Â°C,45.0,%,polyethylene,coated,chitosan,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

74,Barrier properties of chitosan coated polyethylene,,,,,,,,,1.237E-12,gm/m2Pas,5E-05,m,25.0,Â°C,70.0,%,polyethylene,coated,chitosan,"[â€˜CSâ€™, â€™2.0â€™, â€˜%â€™]",glycerol

75,Barrier properties of chitosan coated polyethylene,8.83E-15,gm/m2Pas,,,,,,,,,,,25.0,Â°C,0.0,%,chitosan,individual,None,"[â€˜CSâ€™, â€™1.0â€™, â€˜%â€™]",glycerol

76,Gas separation properties of polyether-based polyurethaneâ€“silica nanocomposite membranes,,,,,1.3986438847302E-07,cm3cm/m2Pas,,,,,0.0001,m,25.0,Â°C,,,polyurethane,individual,None,,

77,Gas separation properties of polyether-based polyurethaneâ€“silica nanocomposite membranes,,,,,9.00076506503053E-08,cm3cm/m2Pas,,,,,0.0001,m,25.0,Â°C,,,polyurethane,nanocomposite,silica,"[â€˜silicaâ€™, â€™20.0â€™, â€™%â€™]",

78,Gas separation properties of polyether-based polyurethaneâ€“silica nanocomposite membranes,1.21960366631164E-08,cm3cm/m2Pas,,,,,,,,,0.0001,m,25.0,Â°C,,,polyurethane,individual,None, ,

79,Gas separation properties of polyether-based polyurethaneâ€“silica nanocomposite membranes,5.76799027917373E-09,cm3cm/m2Pas,,,,,,,,,0.0001,m,25.0,Â°C,,,polyurethane,nanocomposite,silica,"[â€˜silicaâ€™, â€™20.0â€™, â€™%â€™]",

80,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,6E-19,m3m/m2Pas,,,,,,,,,0.0001159,m,25.0,Â°C,50.0,%,SPI,individual,None,,

81,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,8.1E-19,m3m/m2Pas,,,,,,,,,0.0001145,m,25.0,Â°C,50.0,%,SPI,bilayer,corn zein,,glycerol

82,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,3.51E-18,m3m/m2Pas,,,,,,,,,7.65E-05,m,25.0,Â°C,50.0,%,LDPE,individual,None,,

83,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,2.1644E-16,m3m/m2Pas,,,,,,,,,,,,,,,LDPE,individual,None,,

84,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,4.942E-17,m3m/m2Pas,,,,,,,,,,,,,,,HDPE,individual,None,,

85,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,,,,,,,,,9.4E-10,gm/m2Pas,0.0001159,m,25.0,Â°C,50.0,%,SPI,individual,None,,

86,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,,,,,,,,,6.1E-10,gm/m2Pas,0.0001145,m,25.0,Â°C,50.0,%,SPI,bilayer,corn zein,,glycerol

87,Edible oxygen barrier bilayer film pouches from corn zein and soy protein isolate for olive oil packaging,,,,,,,,,1E-12,gm/m2Pas,7.65E-05,m,25.0,Â°C,50.0,%,LDPE,individual,None,,

88,Gas barrier properties of nanocomposites based on in situ polymerized poly(n-butyl methacrylate) in the presence of surface modified montmorillonite,,,,,4.22285894301016E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,poly(n-butyl methacrylate),nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜0.0â€™, â€™%â€™]",

89,Gas barrier properties of nanocomposites based on in situ polymerized poly(n-butyl methacrylate) in the presence of surface modified montmorillonite,,,,,1.84515683833126E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,poly(n-butyl methacrylate),nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜5.0â€™, â€™%â€™]",

90,Gas barrier properties of nanocomposites based on in situ polymerized poly(n-butyl methacrylate) in the presence of surface modified montmorillonite,,,,,2.25019126625763E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,poly(n-butyl methacrylate),nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜5.0â€™, â€™%â€™]",

91,Gas barrier properties of nanocomposites based on in situ polymerized poly(n-butyl methacrylate) in the presence of surface modified montmorillonite,,,,,1.87515938854803E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,poly(n-butyl methacrylate),nanocomposite,montmorillonite,"[â€˜MMTâ€™, â€˜5.0â€™, â€™%â€™]",

92,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,9.3E-11,gm/m2Pas,7.7E-05,m,25.0,Â°C,75.0,%,soluble soybean polysaccharide,individual,None,,"[â€˜GLYâ€™, â€™0.0â€™, â€™%â€™]"

93,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,1.29E-10,gm/m2Pas,7.1E-05,m,25.0,Â°C,75.0,%,soluble soybean polysaccharide,individual,None,,"[â€˜GLYâ€™, â€™20.0â€™, â€™%â€™]"

94,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,2.04E-10,gm/m2Pas,7.3E-05,m,25.0,Â°C,75.0,%,soluble soybean polysaccharide,individual,None,,"[â€˜GLYâ€™, â€™30.0â€™, â€™%â€™]"

95,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,3.28E-10,gm/m2Pas,8.1E-05,m,25.0,Â°C,75.0,%,soluble soybean polysaccharide,individual,None,,"[â€˜GLYâ€™, â€™40.0â€™, â€™%â€™]"

96,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,1.16E-10,gm/m2Pas,5E-05,m,25.0,Â°C,75.0,%,psyllium hydrocolloid,individual,None,,"[â€˜GLYâ€™, â€™15.0â€™, â€™%â€™]"

97,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,1.54E-10,gm/m2Pas,6E-05,m,25.0,Â°C,75.0,%,psyllium hydrocolloid,individual,None,,"[â€˜GLYâ€™, â€™25.0â€™, â€™%â€™]"

98,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,1.88E-10,gm/m2Pas,7.2E-05,m,25.0,Â°C,75.0,%,psyllium hydrocolloid,individual,None,,"[â€˜GLYâ€™, â€™35.0â€™, â€™%â€™]"

99,Soluble soybean polysaccharide A new carbohydrate to make a biodegradable film for sustainable green packaging,,,,,,,,,8.4E-11,gm/m2Pas,7.2E-05,m,25.0,Â°C,75.0,%,cellophane,individual,None,,

100,Barrier and surface properties of chitosan-coated greaseproof paper,1.82763567910373E-11,cm3cm/m2Pas,,,,,,,,,3.5E-06,m,23.0,Â°C,0.0,%,greaseproof paper,coated,chitosan,"[â€˜CSâ€™, â€™5.2â€™, â€˜g/m2â€™]",

101,Barrier and surface properties of chitosan-coated greaseproof paper,2.05609013899169E-11,cm3cm/m2Pas,,,,,,,,,3.5E-06,m,23.0,Â°C,0.0,%,greaseproof paper,coated,chitosan,"[â€˜CSâ€™, â€™5.2â€™, â€˜g/m2â€™]",

102,Barrier and surface properties of chitosan-coated greaseproof paper,7.99590609607881E-12,cm3cm/m2Pas,,,,,,,,,3.5E-06,m,23.0,Â°C,0.0,%,greaseproof paper,coated,chitosan,"[â€˜CSâ€™, â€™5.2â€™, â€˜g/m2â€™]",

103,Barrier and surface properties of chitosan-coated greaseproof paper,1.82763567910373E-17,cm3cm/m2Pas,,,,,,,,,,,27.0,Â°C,65.0,%,chitosan,indiviudal,None,,

104,Barrier and surface properties of chitosan-coated greaseproof paper,,,,,8.11013332602279E-10,cm3cm/m2Pas,,,,,3.5E-06,m,23.0,Â°C,0.0,%,greaseproof paper,coated,chitosan,"[â€˜CSâ€™, â€™5.2â€™, â€˜g/m2â€™]",

105,Barrier and surface properties of chitosan-coated greaseproof paper,,,,,9.709314E-10,cm3cm/m2Pas,,,,,3.5E-06,m,23.0,Â°C,0.0,%,greaseproof paper,coated,chitosan,"[â€˜CSâ€™, â€™5.2â€™, â€˜g/m2â€™]",

106,Application of bioplastics for food packaging,,,,,,,0.0008680555555555,g/m2s,8.23777514168921E-12,gm/m2Pas,2E-05,m,23.0,Â°C,75.0,%,paperboard,coated,PLA,"[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™]",

107,Application of bioplastics for food packaging,,,,,,,0.0007523148148148,g/m2s,7.13940512279763E-12,gm/m2Pas,2E-05,m,23.0,Â°C,75.0,%,paperboard,coated,PLA,"[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™]",

108,Application of bioplastics for food packaging,,,,,,,1.1574074074E-05,g/m2s,1.09837001889194E-13,gm/m2Pas,2E-05,m,23.0,Â°C,75.0,%,paperboard,coated,"PLA, Al2O3","[[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™], [â€˜Al2O3â€™, â€™25.0â€™, â€˜nmâ€™]]",

109,Application of bioplastics for food packaging,,,2.31481481481481E-10,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,paperboard,coated,"PLA, Al2O3","[[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™], [â€˜Al2O3â€™, â€™25.0â€™, â€˜nmâ€™]]",

110,Application of bioplastics for food packaging,,,4.62962962962963E-08,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,paperboard,coated,PLA,"[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™]",

111,Application of bioplastics for food packaging,,,8.125E-08,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

112,Application of bioplastics for food packaging,,,4.86111111111111E-08,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,paperboard,coated,PLA,"[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™]",

113,Application of bioplastics for food packaging,,,2.31481481481481E-09,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,paperboard,coated,"PLA, Al2O3","[[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™], [â€˜Al2O3â€™, â€™25.0â€™, â€˜nmâ€™]]",

114,Application of bioplastics for food packaging,,,1.38888888888889E-09,cm3/m2Pas,,,,,,,2E-05,m,23.0,Â°C,50.0,%,paperboard,coated,"PLA, Al2O3","[[â€˜PLAâ€™, â€™35.0â€™, â€˜g/m2â€™], [â€˜Al2O3â€™, â€™25.0â€™, â€˜nmâ€™]]",

115,Gas permeation properties of poly(lactic acid),,,,,0.013598844,cm3cm/m2Pas,,,,,,,30.0,Â°C,,,polylactic acid,individual,None,,

116,Gas permeation properties of poly(lactic acid),,,,,0.000266644,cm3cm/m2Pas,,,,,,,30.0,Â°C,,,polyethylene terephthalate,individual,None,,

117,Gas permeation properties of poly(lactic acid),0.0043996259999999,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polylactic acid,individual,None,,

118,Gas permeation properties of poly(lactic acid),5.33288E-05,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyethylene terephthalate,individual,None,,

119,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,6.779E-14,molm/m2Pas,,,,,7.35E-05,m,20.0,Â°C,90.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

120,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,1.84E-15,molm/m2Pas,,,,,7.35E-05,m,20.0,Â°C,70.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

121,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,2.7242E-14,molm/m2Pas,,,,,7.35E-05,m,20.0,Â°C,0.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

122,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,7.4E-18,molm/m2Pas,,,,,,,20.0,Â°C,0.0,%,wheat gluten,individual,None,,

123,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,,,,,1.27E-11,molm/m2Pas,7.35E-05,m,25.0,Â°C,100.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

124,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,8.512E-15,molm/m2Pas,,,,,,,,,7.35E-05,m,20.0,Â°C,90.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

125,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,2.7242E-14,molm/m2Pas,,,,,,,,,7.35E-05,m,20.0,Â°C,0.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

126,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,2.22E-15,molm/m2Pas,,,,,,,,,7.35E-05,m,20.0,Â°C,70.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

127,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,2.16E-15,molm/m2Pas,,,,,,,,,7.35E-05,m,20.0,Â°C,0.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

128,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,1.24E-18,molm/m2Pas,,,,,,,,,,,20.0,Â°C,0.0,%,wheat gluten,individual,None,,

129,Gas transfer properties of wheat gluten coated paper adapted to eMAP of fresh parsley,,,,,,,,,3.7E-11,molm/m2Pas,7.35E-05,m,25.0,Â°C,100.0,%,paper,coated,wheat gluten,"[â€˜WGâ€™, â€™20.7â€™, â€˜g/m2â€™]",

130,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,1.5E-13,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,57.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™8.8â€™, â€˜wt%â€™]"

131,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,1.43E-12,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,57.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™0.0â€™, â€˜wt%â€™]"

132,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,4.3E-12,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,90.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™8.8â€™, â€˜wt%â€™]"

133,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,3.1E-13,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,57.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™21.0â€™, â€˜wt%â€™]"

134,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,1.2E-13,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,0.0,%,EVOH,individual,None,,

135,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,1.45E-12,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,57.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™24.3â€™, â€˜wt%â€™]"

136,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,3.7E-13,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,,,starch,individual,None,,"[â€˜sorbitolâ€™,â€™0.0â€™, â€˜wt%â€™]"

137,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,1E-08,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,,,starch,individual,None,,"[â€˜sorbitolâ€™,â€™28.0â€™, â€˜wt%â€™]"

138,Antiplasticisation and oxygen permeability of starchâ€“sorbitol films,9.346E-10,cm3cm/m2Pas,,,,,,,,,0.0005,m,20.0,Â°C,90.0,%,starch,individual,None,,"[â€˜sorbitolâ€™,â€™28.0â€™, â€˜wt%â€™]"

139,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,5.98E-11,gm/m2Pas,1.1E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™1.5â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

140,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,5.14E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

141,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,4.94E-11,gm/m2Pas,1.9E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™4.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

142,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,5.23E-11,gm/m2Pas,2.6E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™5.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

143,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,5.25E-11,gm/m2Pas,2.4E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™6.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

144,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,1.16E-10,gm/m2Pas,2.4E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™75.0â€™, â€˜%â€™]]","[â€˜PEG400â€™,â€™0.66â€™,â€™%â€™]"

145,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,8.29E-11,gm/m2Pas,1.8E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™67.0â€™, â€˜%â€™]]","[â€˜PEG400â€™,â€™0.66â€™,â€™%â€™]"

146,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,7.47E-11,gm/m2Pas,1.8E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]","[â€˜PEG400â€™,â€™0.66â€™,â€™%â€™]"

147,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,7.45E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™25.0â€™, â€˜%â€™]]","[â€˜PEG400â€™,â€™0.66â€™,â€™%â€™]"

148,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,6.97E-11,gm/m2Pas,1.6E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™0.0â€™, â€˜%â€™]]","[â€˜PEG400â€™,â€™0.66â€™,â€™%â€™]"

149,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,1.086E-10,gm/m2Pas,2.3E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™75.0â€™, â€˜%â€™]]",

150,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,6.78E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™67.0â€™, â€˜%â€™]]",

151,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,5.14E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™50.0â€™, â€˜%â€™]]",

152,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,4.24E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™25.0â€™, â€˜%â€™]]",

153,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,2.32E-11,gm/m2Pas,1.5E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™0.0â€™, â€˜%â€™]]",

154,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,7.41E-11,gm/m2Pas,1.6E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™0.0â€™, â€˜%â€™]]","[â€˜PEG1450â€™,â€™0.66â€™,â€™%â€™]"

155,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,7.32E-11,gm/m2Pas,1.6E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™0.0â€™, â€˜%â€™]]","[â€˜PEG4000â€™,â€™0.66â€™,â€™%â€™]"

156,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,6.67E-11,gm/m2Pas,1.7E-05,m,25.0,Â°C,50.0,%,methylcellulose,individual,None,"[[â€˜MCâ€™, â€™3.0â€™, â€™%â€™], [â€˜EtOHâ€™, â€™0.0â€™, â€˜%â€™]]","[â€˜PEG8000â€™,â€™0.66â€™,â€™%â€™]"

157,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,8.7E-13,gm/m2Pas,,,,,,,LDPE,individual,None,,

158,"Water vapor permeability, tensile properties and solubility of methylcellulose-based edible films",,,,,,,,,2.2E-13,gm/m2Pas,,,,,,,HDPE,individual,None,,

159,Barrier and mechanical properties of carrot puree films,2.027E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™, â€™0.3â€™, â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™6.30â€™, â€˜%â€™]"

160,Barrier and mechanical properties of carrot puree films,1.808E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™5.04â€™, â€™%â€™]"

161,Barrier and mechanical properties of carrot puree films,1.486E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™3.78â€™, â€™%â€™]"

162,Barrier and mechanical properties of carrot puree films,1.375E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™2.52â€™, â€˜%â€™]"

163,Barrier and mechanical properties of carrot puree films,1.307E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™1.26â€™, â€˜%â€™]"

164,Barrier and mechanical properties of carrot puree films,1.257E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€™GLYâ€™, â€™0â€™, â€™%â€™]"

165,Barrier and mechanical properties of carrot puree films,,,,,,,,,6.631E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™6.30â€™, â€˜%â€™]"

166,Barrier and mechanical properties of carrot puree films,,,,,,,,,4.886E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™5.04â€™, â€™%â€™]"

167,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.844E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™3.78â€™, â€™%â€™]"

168,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.308E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™2.52â€™, â€˜%â€™]"

169,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.122E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™, â€™1.26â€™, â€˜%â€™]"

170,Barrier and mechanical properties of carrot puree films,,,,,,,,,1.761E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€™GLYâ€™, â€™0â€™, â€™%â€™]"

171,Barrier and mechanical properties of carrot puree films,1.381E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.5â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

172,Barrier and mechanical properties of carrot puree films,1.297E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.4â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

173,Barrier and mechanical properties of carrot puree films,1.397E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

174,Barrier and mechanical properties of carrot puree films,1.338E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.2â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

175,Barrier and mechanical properties of carrot puree films,1.48E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™,â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.1â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

176,Barrier and mechanical properties of carrot puree films,1.457E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.0â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

177,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.872E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.5â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

178,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.414E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.4â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

179,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.156E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

180,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.711E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.2â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

181,Barrier and mechanical properties of carrot puree films,,,,,,,,,3.469E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.1â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

182,Barrier and mechanical properties of carrot puree films,,,,,,,,,3.828E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,gelatin,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.0â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

183,Barrier and mechanical properties of carrot puree films,1.359E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™1.0â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

184,Barrier and mechanical properties of carrot puree films,1.373E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.7â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

185,Barrier and mechanical properties of carrot puree films,1.376E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.5â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

186,Barrier and mechanical properties of carrot puree films,1.398E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

187,Barrier and mechanical properties of carrot puree films,1.425E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.1â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

188,Barrier and mechanical properties of carrot puree films,1.453E-11,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.0â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

189,Barrier and mechanical properties of carrot puree films,,,,,,,,,3.272E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™1.0â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

190,Barrier and mechanical properties of carrot puree films,,,,,,,,,3.153E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.7â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

191,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.689E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.5â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

192,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.442E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.3â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

193,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.286E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.1â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

194,Barrier and mechanical properties of carrot puree films,,,,,,,,,2.181E-09,gm/m2Pas,,,25.0,Â°C,,,carrot puree,blend,CMC,"[[â€˜CMCâ€™,â€™0.0â€™,â€™%â€™], [â€˜corn starchâ€™, â€™3.0â€™,â€™%â€™], [â€˜gelatinâ€™,â€™0.3â€™,â€™%â€™]]","[â€˜GLYâ€™,â€™3.78â€™, â€˜%â€™]"

195,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,,,,,,,1.18333333333333E-10,gm/m2Pas,,,25.0,Â°C,60.0,%,polypropylene,individual,None,,

196,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.0231481481481481,cm3/m2s,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,individual,None,,

197,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.0053935185185185,cm3/m2s,,,,,,,4E-06,m,23.0,Â°C,0.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€™15.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€™0.2â€™, â€™%â€™]"

198,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.009386574074074,cm3/m2s,,,,,,,4E-06,m,23.0,Â°C,0.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€˜5.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€™0.2â€™, â€™%â€™]"

199,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.0099305555555555,cm3/m2s,,,,,,,4E-06,m,23.0,Â°C,0.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€™5.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€™0.5â€™, â€™%â€™]"

200,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.007048611111111,cm3/m2s,,,,,,,4E-06,m,23.0,Â°C,0.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€˜5.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€™0.2â€™, â€™%â€™]"

201,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,0.0056481481481481,cm3/m2s,,,,,,,4E-06,m,23.0,Â°C,0.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€™5.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€™0.5â€™, â€™%â€™]"

202,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,,,,,,,2.51666666666667E-11,gm/m2Pas,4E-06,m,25.0,Â°C,60.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€˜5.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€™0.2â€™, â€™%â€™]"

203,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,,,,,,,1.1E-10,gm/m2Pas,4E-06,m,25.0,Â°C,60.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€™5.0â€™, â€™%â€™]","[â€˜PEGâ€™, â€™0.5â€™, â€™%â€™]"

204,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,,,,,,,1.58333333333333E-11,gm/m2Pas,4E-06,m,25.0,Â°C,60.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€˜5.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€™0.2â€™, â€™%â€™]"

205,Water vapor and oxygen-barrier performance of cornâ€“zein coated polypropylene films,,,,,,,,,3.58333333333333E-11,gm/m2Pas,4E-06,m,25.0,Â°C,60.0,%,polypropylene,coated,cornâ€“zein,"[â€˜CZâ€™, â€™5.0â€™, â€™%â€™]","[â€˜GLYâ€™, â€™0.5â€™, â€™%â€™]"

206,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.53009259259259E-10,gm/m2Pas,,,,,,,chitosan,individual,None,,

207,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,9.07407407407407E-11,gm/m2Pas,,,,,90.0,%,chitosan,individual,None,,"[â€˜GLYâ€™, â€™0.4â€™, â€™%â€™]"

208,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.04166666666667E-10,gm/m2Pas,,,,,90.0,%,chitosan,individual,None,,"[â€˜sorbitolâ€™,â€™0.1â€™,â€™%â€™]"

209,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.88657407407407E-10,gm/m2Pas,,,,,90.0,%,chitosan,individual,None,,"[â€˜sorbitolâ€™, â€™0.5â€™, â€™%â€™]"

210,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,2.19907407407407E-10,gm/m2Pas,,,,,90.0,%,chitosan,individual,None,,"[â€˜PEGâ€™, â€™0.2â€™, â€™%â€™]"

211,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.14227229943983E-11,gm/m2Pas,,,23.0,â„ƒ,50.0,%,chitosan,individual,None,,"[â€˜GLYâ€™, â€™0.25â€™, â€™mL/gâ€™]"

212,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,8.6812694757427E-12,gm/m2Pas,,,23.0,â„ƒ,50.0,%,chitosan,individual,None,,"[â€˜GLYâ€™, â€™0.25â€™, â€™mL/gâ€™]"

213,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.56481481481482E-10,gm/m2Pas,,,,,90.0,%,chitosan,blend,stearic acid,"[â€˜FAâ€™, â€™0.5â€™, â€™%â€™]",fatty acid

214,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,,,,,,,1.66898148148148E-10,gm/m2Pas,,,,,90.0,%,chitosan,blend,palmitic acid,"[â€˜FAâ€™, â€™0.5â€™, â€™%â€™]",fatty acid

215,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,3.7037037037037E-06,cm3cm/m2Pas,,,,,,,,,,,,,chitosan,individual,None,,

216,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,7.39583333333333E-08,cm3cm/m2Pas,,,,,,,,,,,,,chitosan,blend,palmitic acid,"[â€˜FAâ€™, â€™0.1â€™, â€™%â€™]",fatty acid

217,Effect of plasticizers and fatty acids on mechanical and permeability characteristics of chitosan films,,,2.70833333333333E-08,cm3cm/m2Pas,,,,,,,,,23.0,â„ƒ,60.0,%,chitosan,blend,palmitic acid,,fatty acid

218,Gas permeation and mechanical properties of polypropylene nanocomposites with thermally-stable imidazolium modified clay,1.3733400462963E-05,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,individual,None,"[â€˜OMMTâ€™, â€˜0.0â€™, â€˜%â€™]",

219,Gas permeation and mechanical properties of polypropylene nanocomposites with thermally-stable imidazolium modified clay,1.09558587962963E-05,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜1.0â€™, â€˜%â€™]",

220,Gas permeation and mechanical properties of polypropylene nanocomposites with thermally-stable imidazolium modified clay,9.41278009259263E-06,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜2.0â€™, â€˜%â€™]",

221,Gas permeation and mechanical properties of polypropylene nanocomposites with thermally-stable imidazolium modified clay,8.17831712962966E-06,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.0â€™, â€˜%â€™]",

222,Gas permeation and mechanical properties of polypropylene nanocomposites with thermally-stable imidazolium modified clay,7.40677777777778E-06,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,polypropylene,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜4.0â€™, â€˜%â€™]",

223,Design of biodegradable bio-based equilibrium modified atmosphere packaging (EMAP) for fresh fruits and vegetables by using micro-perforated poly-lactic acid (PLA) films,,,,,4.4E-09,gm/m2s,,,,,3E-05,m,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

224,Design of biodegradable bio-based equilibrium modified atmosphere packaging (EMAP) for fresh fruits and vegetables by using micro-perforated poly-lactic acid (PLA) films,,,,,2.77E-14,gm/m2Pas,,,,,3E-05,m,25.0,Â°C,0.0,%,polylactic acid,individual,None,,

225,Design of biodegradable bio-based equilibrium modified atmosphere packaging (EMAP) for fresh fruits and vegetables by using micro-perforated poly-lactic acid (PLA) films,,,,,1.99E-14,gm/m2Pas,,,,,3E-05,m,25.0,Â°C,0.0,%,polylactic acid,individual,None,,

226,Design of biodegradable bio-based equilibrium modified atmosphere packaging (EMAP) for fresh fruits and vegetables by using micro-perforated poly-lactic acid (PLA) films,5.3E-09,gm/m2s,,,,,,,,,3E-05,m,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

227,Design of biodegradable bio-based equilibrium modified atmosphere packaging (EMAP) for fresh fruits and vegetables by using micro-perforated poly-lactic acid (PLA) films,,,,,,,,,1.4E-06,gm/m2s,3E-05,m,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

228,Effect of an organo-modified montmorillonite on PLA crystallization and gas barrier properties,3.750916E-10,cm3cm/m2Pas,,,,,,,,,1E-04,m,20.0,Â°C,,,polylactic acid,individual,None,,

229,Effect of an organo-modified montmorillonite on PLA crystallization and gas barrier properties,3.15077E-10,cm3cm/m2Pas,,,,,,,,,1E-04,m,20.0,Â°C,,,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.8â€™, â€˜%â€™]",

230,Effect of an organo-modified montmorillonite on PLA crystallization and gas barrier properties,2.85035E-10,cm3cm/m2Pas,,,,,,,,,1E-04,m,20.0,Â°C,,,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜7.9â€™, â€˜%â€™]",

231,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,1.04E-11,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,individual,None,,

232,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,1E-11,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,nanocomposite,Ag,"[â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]",

233,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,6.6E-12,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,nanocomposite,"CNC, Ag","[[â€˜CNCâ€™, â€˜1.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

234,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,4.3E-12,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,nanocomposite,"sCNC, Ag","[[â€˜sCNCâ€™, â€˜1.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

235,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,5.5E-12,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,nanocomposite,"CNC, Ag","[[â€˜CNCâ€™, â€˜5.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

236,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,,,,,,,4.3E-12,gm/m2Pas,2.1E-04,m,20.0,Â°C,50.0,%,polylactic acid,nanocomposite,"sCNC, Ag","[[â€˜sCNCâ€™, â€˜5.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

237,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,3.5300926E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,individual,None,,

238,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,2.7662037E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,nanocomposite,Ag,"[â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]",

239,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,1.9097222E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,nanocomposite,"CNC, Ag","[[â€˜CNCâ€™, â€˜1.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

240,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,1.6435185E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,nanocomposite,"sCNC, Ag","[[â€˜sCNCâ€™, â€˜1.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

241,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,2.0601852E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,nanocomposite,"CNC, Ag","[[â€˜CNCâ€™, â€˜5.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

242,Combined effects of cellulose nanocrystals and silver nanoparticles on the barrier and migration properties of PLA nano-biocomposites,,,1.4583333E-05,cm3cm/m2s,,,,,,,2.1E-04,m,25.0,Â°C,,,polylactic acid,nanocomposite,"sCNC, Ag","[[â€˜sCNCâ€™, â€˜5.0â€™, â€˜%â€™], [â€˜Agâ€™, â€˜1.0â€™, â€˜%â€™]]",

243,Mechanical properties and water vapor permeability of edible films made from fractionated soy proteins with ultrafiltration,,,,,,,,,8.3E-10,gm/m2Pas,6.77E-05,m,25.0,Â°C,50.0,%,SPI,individual,None,,

244,Mechanical properties and water vapor permeability of edible films made from fractionated soy proteins with ultrafiltration,,,,,,,,,8.3E-10,gm/m2Pas,6.15E-05,m,25.0,Â°C,50.0,%,SPI,individual,None,,

245,Mechanical properties and water vapor permeability of edible films made from fractionated soy proteins with ultrafiltration,,,,,,,,,8.5E-10,gm/m2Pas,6.86E-05,m,25.0,Â°C,50.0,%,SPI,individual,None,,

246,Mechanical properties and water vapor permeability of edible films made from fractionated soy proteins with ultrafiltration,,,,,,,,,8E-10,gm/m2Pas,6.59E-05,m,25.0,Â°C,50.0,%,SPI,individual,None,,

247,Improve the gas barrier property of PET film with montmorillonite by in situ interlayer polymerization,8.6259259E-13,cm3cm/m2Pas,,,,,,,,,2.5E-05,m,,,,,polyethylene terephthalate,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜0.0â€™, â€˜%â€™]",

248,Improve the gas barrier property of PET film with montmorillonite by in situ interlayer polymerization,6.3824074E-13,cm3cm/m2Pas,,,,,,,,,2.5E-05,m,,,,,polyethylene terephthalate,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜1.0â€™, â€˜%â€™]",

249,Improve the gas barrier property of PET film with montmorillonite by in situ interlayer polymerization,5.321037E-13,cm3cm/m2Pas,,,,,,,,,2.5E-05,m,,,,,polyethylene terephthalate,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜2.0â€™, â€˜%â€™]",

250,Improve the gas barrier property of PET film with montmorillonite by in situ interlayer polymerization,4.340278E-13,cm3cm/m2Pas,,,,,,,,,2.5E-05,m,,,,,polyethylene terephthalate,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.0â€™, â€˜%â€™]",

251,"Effect of lignin on water vapor barrier, mechanical, and structural properties of agar-lignin composite films",,,,,,,,,2.11E-09,gm/m2Pas,6.05E-05,m,25.0,Â°C,50.0,%,agar,individual,None,,

252,"Effect of lignin on water vapor barrier, mechanical, and structural properties of agar-lignin composite films",,,,,,,,,1.97E-09,gm/m2Pas,6.03E-05,m,25.0,Â°C,50.0,%,agar,blend,lignin,"[â€˜ligninâ€™, â€˜1.0â€™, â€˜%â€™]",glycerol

253,"Effect of lignin on water vapor barrier, mechanical, and structural properties of agar-lignin composite films",,,,,,,,,1.89E-09,gm/m2Pas,6.11E-05,m,25.0,Â°C,50.0,%,agar,blend,lignin,"[â€˜ligninâ€™, â€˜3.0â€™, â€˜%â€™]",glycerol

254,"Effect of lignin on water vapor barrier, mechanical, and structural properties of agar-lignin composite films",,,,,,,,,1.77E-09,gm/m2Pas,5.71E-05,m,25.0,Â°C,50.0,%,agar,blend,lignin,"[â€˜ligninâ€™, â€˜5.0â€™, â€˜%â€™]",glycerol

255,"Effect of lignin on water vapor barrier, mechanical, and structural properties of agar-lignin composite films",,,,,,,,,1.53E-09,gm/m2Pas,5.78E-05,m,25.0,Â°C,50.0,%,agar,blend,lignin,"[â€˜ligninâ€™, â€™10.0â€™, â€˜%â€™]",glycerol

256,Oxygen permeability and mechanical properties of banana films,7.87037E-12,cm3cm/m2Pas,,,,,,,,,1E-04,m,25.0,Â°C,0.0,%,methylcellulose,individual,None,,

257,Oxygen permeability and mechanical properties of banana films,6.828703E-10,cm3cm/m2Pas,,,,,,,,,1E-04,m,23.0,Â°C,50.0,%,denatured whey protein isolate,individual,None,,

258,Oxygen permeability and mechanical properties of banana films,9.027777E-10,cm3cm/m2Pas,,,,,,,,,1E-04,m,23.0,Â°C,50.0,%,whey protein isolate,individual,None,,

259,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,5.2034722E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,individual,None,,

260,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,4.58611109E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜1.0â€™, â€˜%â€™]",

261,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,4.08634257E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜2.0â€™, â€˜%â€™]",

262,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,3.70416665E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.0â€™, â€˜%â€™]",

263,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,3.35138887E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜4.0â€™, â€˜%â€™]",

264,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,3.14560184E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜5.0â€™, â€˜%â€™]",

265,Water vapour permeability of poly(lactic acid) nanocomposites,,,,,,,2.96921295E-06,g/m2s,,,6E-04,m,38.0,Â°C,90.0,%,polylactic acid,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜6.0â€™, â€˜%â€™]",

266,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,1.1072E-08,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,individual,None,,

267,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,9.151E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜1.0â€™, â€˜%â€™]",

268,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,7.949E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.0â€™, â€˜%â€™]",

269,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,7.907E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜5.0â€™, â€˜%â€™]",

270,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,8.371E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜1.0â€™, â€˜%â€™]",

271,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,7.073E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜3.0â€™, â€˜%â€™]",

272,Synthesis of chain-extended organifier and properties of polyurethane clay nanocomposites,6.49E-09,cm3cm/m2Pas,,,,,,,,,,,30.0,Â°C,,,polyurethane,nanocomposite,OMMT,"[â€˜OMMTâ€™, â€˜5.0â€™, â€˜%â€™]",

273,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,,,,,3.375E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,polysulfone,individual,None,,

274,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,,,,,4.950396E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '10.0â€™, â€˜%â€™]",

275,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,,,,,5.850468E-08,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '20.0â€™, â€˜%â€™]",

276,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,,,,,1.1100888E-07,cm3cm/m2Pas,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '40.0â€™, â€˜%â€™]",

277,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,7.350588E-09,cm3cm/m2Pas,,,,,,,,,,,25.0,Â°C,,,polysulfone,individual,None,,

278,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,1.050084E-08,cm3cm/m2Pas,,,,,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '10.0â€™, â€˜%â€™]",

279,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,1.275103E-08,cm3cm/m2Pas,,,,,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '20.0â€™, â€˜%â€™]",

280,High permeability nano-composite membranes based on mesoporous MCM-41 nanoparticles in a polysulfone matrix,2.550204E-08,cm3cm/m2Pas,,,,,,,,,,,25.0,Â°C,,,polysulfone,nanocomposite,silica,"[â€˜silicaâ€™, '40.0â€™, â€˜%â€™]",

281,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,4.6296E-08,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,microfibrillated cellulose,individual,None,,

282,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,1.1574E-05,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polyethylene terephthalate,individual,None,,

283,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,5.787E-05,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polyethylene terephthalate,individual,None,,

284,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,5.787E-04,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polypropylene,individual,None,,

285,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,1.1574E-03,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polypropylene,individual,None,,

286,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,1.1574E-13,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polyvinylidene chloride,individual,None,,

287,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,3.4722E-12,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polyvinylidene chloride,individual,None,,

288,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,2.581002E-08,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,0.0,%,EVOH,individual,None,,

289,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,1.956006E-10,cm3cm/m2Pas,,,,,,,,,,,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

290,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,1.81712E-04,gm/m2Pas,,,23.0,Â°C,50.0,%,microfibrillated cellulose,individual,None,,

291,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,1.504629E-10,gm/m2Pas,,,21.0,Â°C,60.0,%,polyethylene terephthalate,individual,None,,

292,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,5.70601852E-06,gm/m2Pas,,,37.8,Â°C,90.0,%,polypropylene,individual,None,,

293,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,8.0902778E-06,gm/m2Pas,,,23.0,Â°C,45.0,%,polyvinylidene chloride,individual,None,,

294,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,1.0995374E-06,gm/m2Pas,,,23.0,Â°C,95.0,%,EVOH,individual,None,,

295,The effect of pre-treatment and process conditions on the gas barrier properties of fibrillated cellulose films and coatings: A review,,,,,,,,,4.46759259E-06,gm/m2Pas,,,23.0,Â°C,50.0,%,polylactic acid,individual,None,,

Supplementary Figure 1. GMM model clustering outcome with 6 distinct clusters

Supplementary Figure 2. K-Means model clustering outcome with 6 distinct clusters,

Supplementary Figure 3. Silhouette Score Analysis for Optimal Cluster Determination in K-Means and Gaussian Mixture Models. Both algorithms achieve their highest silhouette score when the number of clusters is set to 6, indicating that 6 clusters is the optimal configuration for each model.

Supplementary Figure 4. K-Distance Plot for Determining DBSCAN ε Parameter. The “elbow” observed at the 245th point corresponds to an ε value of 1.17, which was selected as the optimal neighborhood radius for the DBSCAN clustering algorithm.

The Python code is available as below:

import os

import pandas as pd

import numpy as np

import plotly

import plotly.express as px

import plotly.graph_objects as go

combined_dataframe = pd.read_csv('semi-processed_2.csv')

combined_dataframe['Type'] = combined_dataframe['Type'].replace('Individual', 'individual')

combined_dataframe['Secondary Material'] = combined_dataframe['Secondary Material'].fillna('None')

combined_dataframe['Composition'] = combined_dataframe['Composition'].fillna('None')

columns_to_drop = ['OP_Num', 'OTR_Num', 'PCO2_Num', 'WVP_Num', 'WVTR_Num']

combined_dataframe = combined_dataframe.drop(columns=[col for col in columns_to_drop if col in combined_dataframe.columns], errors='ignore')

# combined_dataframe.to_csv('semi-processed.csv')

value_counts = combined_dataframe[['OP_Unit', 'OTR_Unit', 'WVP_Unit', 'WVTR_Unit']].apply(pd.Series.value_counts)

print(value_counts)

OP_Unit  OTR_Unit  WVP_Unit  WVTR_Unit

cm3/m2Pas        NaN       6.0       NaN        NaN

cm3/m2s          NaN       6.0       NaN        NaN

cm3cm/m2Pas     80.0       3.0       NaN        NaN

cm3cm/m2s        NaN       6.0       NaN        NaN

g/m2s            NaN       NaN       NaN       10.0

gm/m2Pas        11.0       NaN     134.0        NaN

gm/m2s           1.0       NaN       1.0        NaN

m3m/m2Pas        5.0       NaN       NaN        NaN

molm/m2Pas       5.0       NaN       2.0        NaN

# combined_dataframe.drop(columns='Doc')

# combined_dataframe = combined_dataframe[['Base Material', 'Type', 'Secondary Material',

#                                          'OP_Updated_Num', 'OP_Unit', 'OTR_Updated_Num', 'OTR_Unit',

#                                          'PCO2_Updated_Num', 'PCO2_Unit',

#                                          'WVTR_Updated_Num', 'WVTR_Unit', 'WVP_Updated_Num', 'WVP_Unit',

#                                          'thickness_Updated_Num', 'thickness_Unit',

#                                          'temperature_Updated_Num', 'temperature_Unit',

#                                          'RH_Updated_Num', 'RH_Unit',

#                                          'Composition', 'Plasticizer']]

# combined_dataframe.to_csv('FE.csv')

# Apply the conversion where 'OP_Unit' is 'gm/m2Pas'

# Mass-to-volume

condition_o2g2cm = combined_dataframe['OP_Unit'] == 'gm/m2Pas'

combined_dataframe.loc[condition_o2g2cm, 'OP_Updated_Num'] *= 100/0.001429

combined_dataframe.loc[condition_o2g2cm, 'OP_Unit'] = 'cm3cm/m2Pas'

condition_o2m2cm = combined_dataframe['OP_Unit'] == 'm3m/m2Pas'

combined_dataframe.loc[condition_o2m2cm, 'OP_Updated_Num'] *= 100000000

combined_dataframe.loc[condition_o2m2cm, 'OP_Unit']  = 'cm3cm/m2Pas'

# o2 : 0.0014g/cm3, co2 : 0.001836 g/cm3

# Mass-to-volume

condition_o2m2cmg2cm = combined_dataframe['OP_Unit'] == 'gm/m2s'

combined_dataframe.loc[condition_o2m2cmg2cm, 'OP_Updated_Num'] *= 100/0.001429

combined_dataframe.loc[condition_o2m2cmg2cm,'OP_Unit'] = 'cm3cm/m2s'

# Mass-to-volume

condition_co2g2cm = combined_dataframe['PCO2_Unit'] == 'gm/m2Pas'

combined_dataframe.loc[condition_co2g2cm, 'OP_Updated_Num'] *= 100/0.001836

combined_dataframe.loc[condition_co2g2cm, 'PCO2_Unit'] = 'cm3cm/m2Pas'

condition_o2mol2cm = combined_dataframe['OP_Unit'] == 'molm/m2Pas'

combined_dataframe.loc[condition_o2mol2cm, 'OP_Updated_Num'] *= 116059.480952

combined_dataframe.loc[condition_o2mol2cm, 'OP_Unit'] = 'cm3cm/m2Pas'

# 116059.480952 = 8.314*293.15*1000/21

condition_co2mol2cm = combined_dataframe['PCO2_Unit'] == 'molm/m2Pas'

combined_dataframe.loc[condition_co2mol2cm, 'PCO2_Updated_Num'] *= 116059.480952

combined_dataframe.loc[condition_co2mol2cm, 'PCO2_Unit'] = 'cm3cm/m2Pas'

# molecular weight of water (18.0153 g/mol) converts

condition_wmol2g = combined_dataframe['WVP_Unit'] == 'molm/m2Pas'

combined_dataframe.loc[condition_wmol2g, 'WVP_Updated_Num'] *= 18.0153

combined_dataframe.loc[condition_wmol2g, 'WVP_Unit'] = 'gm/m2Pas'

#875448000000000

condition_o2 = combined_dataframe['OP_Unit'] == 'cm3cm/m2Pas'

combined_dataframe.loc[condition_o2, 'OP_Updated_Num'] *= 10000*86400*101325

combined_dataframe.loc[condition_o2, 'OP_Unit'] = 'cm3um/m2dayatm'

condition_wPa2kPa = combined_dataframe['WVP_Unit'] == 'gm/m2Pas'

combined_dataframe.loc[condition_wPa2kPa, 'WVP_Updated_Num'] *= 86400*1000000*1000

combined_dataframe.loc[condition_wPa2kPa, 'WVP_Unit'] = 'gum/m2daykPa'

combined_dataframe['thickness_Updated_Num'] = combined_dataframe['thickness_Updated_Num'].fillna(0.0001)

combined_dataframe['thickness_Unit'] = combined_dataframe['thickness_Unit'].fillna('m')

def calculate_otr(row):

# under 1 atm and

if pd.notnull(row['OP_Updated_Num']) and row['OP_Unit'] == 'cm3um/m2dayatm':

row['OTR_Updated_Num'] = row['OP_Updated_Num'] / (row['thickness_Updated_Num'] * 10**6)

row['OTR_Unit'] = 'cm3/m2day'

if pd.notnull(row['OP_Updated_Num']) and row['OP_Unit'] == 'cm3cm/m2s':

row['OTR_Updated_Num'] = row['OP_Updated_Num'] / row['thickness_Updated_Num'] * 864

row['OTR_Unit'] = 'cm3/m2day'

return row

def calculate_wvtr(row):

if pd.notnull(row['WVP_Updated_Num']) and row['WVP_Unit'] == 'gum/m2daykPa':

row['WVTR_Updated_Num'] = (row['WVP_Updated_Num'] * 101.325) / (row['thickness_Updated_Num'] * 10**6)

row['WVTR_Unit'] = 'g/m2day'

return row

combined_dataframe = combined_dataframe.apply(calculate_otr, axis=1).apply(calculate_wvtr, axis=1)

# combined_dataframe = combined_dataframe.apply(calculate_wvtr, axis=1)

def convert_otr(row):

if pd.notnull(row['OTR_Updated_Num']):

if row['OTR_Unit'] == 'cm3/m2s':

row['OTR_Updated_Num'] *= 86400

row['OTR_Unit'] = 'cm3/m2day'

elif row['OTR_Unit'] == 'cm3cm/m2s':

row['OTR_Updated_Num'] = (row['OTR_Updated_Num'] * 864) / row['thickness_Updated_Num']

row['OTR_Unit'] = 'cm3/m2day'

elif row['OTR_Unit'] == 'cm3/m2Pas':

row['OTR_Updated_Num'] = row['OTR_Updated_Num'] * 101325 * 86400

row['OTR_Unit'] = 'cm3/m2day'

elif row['OTR_Unit'] == 'cm3cm/m2Pas':

row['OTR_Updated_Num'] = row['OTR_Updated_Num'] * 101325 * 864 / row['thickness_Updated_Num']

row['OTR_Unit'] = 'cm3/m2day'

return row

def convert_wvtr(row):

if pd.notnull(row['WVTR_Updated_Num']):

if row['WVTR_Unit'] == 'g/m2s':

row['WVTR_Updated_Num'] *= 86400

row['WVTR_Unit'] = 'g/m2day'

return row

combined_dataframe = combined_dataframe.apply(convert_otr, axis=1).apply(convert_wvtr, axis=1)

# combined_dataframe.to_csv('after FE.csv')

combined_dataframe.columns

Index(['Unnamed: 0', 'Doc', 'OP_Updated_Num', 'OP_Unit', 'OTR_Updated_Num',

'OTR_Unit', 'PCO2_Updated_Num', 'PCO2_Unit', 'WVTR_Updated_Num',

'WVTR_Unit', 'WVP_Updated_Num', 'WVP_Unit', 'thickness_Updated_Num',

'thickness_Unit', 'temperature_Updated_Num', 'temperature_Unit',

'RH_Updated_Num', 'RH_Unit', 'Base Material', 'Type',

'Secondary Material', 'Composition', 'Plasticizer'],

dtype='object')

columns = ['OP_Updated_Num', 'OTR_Updated_Num', 'PCO2_Updated_Num', 'WVTR_Updated_Num', 'WVP_Updated_Num']

# Calculate summary statistics

summary_stats = combined_dataframe[columns].describe().transpose()

# Add median to the summary statistics

# Display the summary statistics

print(summary_stats.round(3))

count          mean           std    min       25%  \

OP_Updated_Num    102.0  3.095102e+19  3.117824e+20  0.000   436.266

OTR_Updated_Num   123.0  2.566670e+17  2.839233e+18  0.000    11.578

PCO2_Updated_Num   29.0  0.000000e+00  3.000000e-03  0.000     0.000

WVTR_Updated_Num  143.0  1.231641e+08  1.331648e+09  0.257  1038.401

WVP_Updated_Num   137.0  1.268580e+08  1.342661e+09  0.000  1131.840

50%         75%           max

OP_Updated_Num     2644.110  680038.989  3.148917e+21

OTR_Updated_Num     249.533    5936.851  3.148917e+19

PCO2_Updated_Num      0.000       0.000  1.400000e-02

WVTR_Updated_Num  19251.750  107901.772  1.590794e+10

WVP_Updated_Num    6324.480   57591.311  1.569992e+10

from matplotlib.ticker import FuncFormatter

import matplotlib.pyplot as plt

import numpy as np

import pandas as pd

# Example combined_dataframe setup (replace this with your actual data)

# combined_dataframe = pd.DataFrame({...})

# List of columns to visualize

coll = [ 'OTR', 'WVTR']

text = '_Updated_Num'

u = '_Unit'

columns = [c + text for c in coll]

# Create subplots

fig, axes = plt.subplots(nrows=len(coll), ncols=1, figsize=(8, len(columns) * 4))

all_data = pd.concat([combined_dataframe[col].dropna() for col in columns])

log_all_data = np.log1p(all_data)  # Log-transform combined data for bin calculation

bins = np.linspace(log_all_data.min(), log_all_data.max(), 30)

# Formatter to convert log scale to powers of 10

def log_to_power_of_10(x, pos):

return f"$10^{{{int(x)}}}$"

formatter = FuncFormatter(log_to_power_of_10)

for i, col in enumerate(columns):

# Get the corresponding unit column

unit_column = col.replace(text, u)

# Find the most common unit

if unit_column in combined_dataframe:

most_common_unit = combined_dataframe[unit_column].value_counts().idxmax()

else:

most_common_unit = "unknown"  # Fallback if the unit column doesn't exist

# Drop NaN values and apply log transformation (add 1 to avoid log(0))

data = combined_dataframe[col].dropna()

log_data = np.log1p(data)  # log1p handles log(1 + x)

# Plot histogram

axes[i].hist(log_data, bins=bins, color='skyblue', edgecolor='black')

axes[i].set_xlabel(f"{col.split('_')[0]} ({most_common_unit})")  # Set x-label with unit

axes[i].set_ylabel('Frequency')

# Apply custom formatter to x-axis

axes[i].xaxis.set_major_formatter(formatter)

plt.tight_layout()

plt.suptitle('Gas Permeability Distributions', y=1.02, fontsize=14)

plt.show()

# Create new columns for OP temperature

combined_dataframe['OTR_temperature_Num'] = combined_dataframe.apply(

lambda row: row['temperature_Updated_Num'] if pd.notnull(row['OTR_Updated_Num']) else None, axis=1)

combined_dataframe['OTR_temperature_Unit'] = combined_dataframe.apply(

lambda row: row['temperature_Unit'] if pd.notnull(row['OTR_Updated_Num']) else None, axis=1)

combined_dataframe['OTR_RH_Num'] = combined_dataframe.apply(

lambda row: row['RH_Updated_Num'] if pd.notnull(row['OTR_Updated_Num']) else None, axis=1)

combined_dataframe['OTR_RH_Unit'] = combined_dataframe.apply(

lambda row: row['RH_Unit'] if pd.notnull(row['OTR_Updated_Num']) else None, axis=1)

# Create new columns for WVP temperature

combined_dataframe['WVTR_temperature_Num'] = combined_dataframe.apply(

lambda row: row['temperature_Updated_Num'] if pd.notnull(row['WVTR_Updated_Num']) else None, axis=1)

combined_dataframe['WVTR_temperature_Unit'] = combined_dataframe.apply(

lambda row: row['temperature_Unit'] if pd.notnull(row['WVTR_Updated_Num']) else None, axis=1)

combined_dataframe['WVTR_RH_Num'] = combined_dataframe.apply(

lambda row: row['RH_Updated_Num'] if pd.notnull(row['WVTR_Updated_Num']) else None, axis=1)

combined_dataframe['WVTR_RH_Unit'] = combined_dataframe.apply(

lambda row: row['RH_Unit'] if pd.notnull(row['WVTR_Updated_Num']) else None, axis=1)

combined_dataframe['Type'] = combined_dataframe['Type'].replace('Individual', 'individual')

conventional_materials = ['polypropylene', 'polyethylene', 'polyvinyl chloride', 'LDPE', 'HDPE', 'poly(n-butyl methacrylate)', 'polyethylene terephthalate', 'EVOH', 'polysulfone']

# Create a new column 'Material' based on the condition

combined_dataframe['Material'] = combined_dataframe['Base Material'].apply(lambda x: 'conventional' if x in conventional_materials else 'sustainable')

col = ['Base Material', 'Type', 'Secondary Material','Material']

otr = combined_dataframe.filter(regex='^OTR', axis=1)

op = combined_dataframe.filter(regex='^OP', axis=1)

wvp = combined_dataframe.filter(regex='^WVP', axis=1)

wvtr = combined_dataframe.filter(regex='^WVTR', axis=1)

op[col] = combined_dataframe[col]

otr[col] = combined_dataframe[col]

wvp[col] = combined_dataframe[col]

wvtr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:8: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

op[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:8: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

op[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:8: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

op[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:8: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

op[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:9: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

otr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:9: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

otr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:9: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

otr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:9: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

otr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:10: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvp[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:10: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvp[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:10: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvp[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:10: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvp[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:11: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvtr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:11: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvtr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:11: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvtr[col] = combined_dataframe[col]

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1357264389.py:11: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

wvtr[col] = combined_dataframe[col]

fop = op[op['OP_Updated_Num'].notnull()]

fotr = otr[otr['OTR_Updated_Num'].notnull()]

fwvp = wvp[wvp['WVP_Updated_Num'].notnull()]

fwvtr = wvtr[wvtr['WVTR_Updated_Num'].notnull()]

fotr['OTR_temperature_Num'] = fotr['OTR_temperature_Num'].fillna(23.0)

fotr['OTR_RH_Num'] = fotr['OTR_RH_Num'].fillna(50.0)

fwvtr['WVTR_temperature_Num'] = fwvtr['WVTR_temperature_Num'].fillna(25.0)

fwvtr['WVTR_RH_Num'] = fwvtr['WVTR_RH_Num'].fillna(50.0)

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/4199108202.py:1: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

fotr['OTR_temperature_Num'] = fotr['OTR_temperature_Num'].fillna(23.0)

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/4199108202.py:2: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

fotr['OTR_RH_Num'] = fotr['OTR_RH_Num'].fillna(50.0)

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/4199108202.py:3: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

fwvtr['WVTR_temperature_Num'] = fwvtr['WVTR_temperature_Num'].fillna(25.0)

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/4199108202.py:4: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

fwvtr['WVTR_RH_Num'] = fwvtr['WVTR_RH_Num'].fillna(50.0)

print('fotr before', len(fotr))

fotr = fotr[(fotr['OTR_temperature_Num'] == 23.0) & (fotr['OTR_RH_Num'] == 50.0)]

print('fotr after', len(fotr))

print('fwvtr after', len(fwvtr))

fwvtr = fwvtr[(fwvtr['WVTR_temperature_Num'] == 25.0) & (fwvtr['WVTR_RH_Num'] == 50.0)]

print('fwvtr after', len(fwvtr))

fotr before 123

fotr after 51

fwvtr after 143

fwvtr after 72

combine_df_tr = pd.merge(fotr, fwvtr, on=col, how='outer')

dtr = combine_df_tr[['WVTR_Updated_Num','OTR_Updated_Num'] + col]

fotr['OTR_Updated_Num'].describe()

count    5.100000e+01

mean     3.105970e+07

std      1.572773e+08

min      1.013244e-01

25%      3.030175e+00

50%      1.223001e+01

75%      5.116912e+02

max      1.013244e+09

Name: OTR_Updated_Num, dtype: float64

fwvtr['WVTR_Updated_Num'].describe()

count        72.000000

mean     101134.975836

std      126553.201389

min          19.259856

25%        1920.514050

50%       38250.962338

75%      200608.909200

max      580509.568800

Name: WVTR_Updated_Num, dtype: float64

# Load datasets

data = fotr  # Replace with your dataset filename

fotr['OTR_temperature_Num'] = fotr['OTR_temperature_Num'].fillna(23.0)

fotr['OTR_RH_Num'] = fotr['OTR_RH_Num'].fillna(50.0)

fotr['OTR_temperature_Num'].describe()

count    51.0

mean     23.0

std       0.0

min      23.0

25%      23.0

50%      23.0

75%      23.0

max      23.0

Name: OTR_temperature_Num, dtype: float64

from matplotlib.ticker import FuncFormatter

import matplotlib.pyplot as plt

import numpy as np

import pandas as pd

# List of columns to visualize

coll = ['OTR', 'WVTR']

text = '_Updated_Num'

u = '_Unit'

columns = [c + text for c in coll]

# Create the figure

fig, ax = plt.subplots(figsize=(8, 6))

# Formatter to convert log scale to powers of 10

def log_to_power_of_10(x, pos):

return f"$10^{{{int(x)}}}$"

formatter = FuncFormatter(log_to_power_of_10)

# Data preparation for OTR and WVTR

combined_data = []

labels = []

for col in columns:

# Initialize data for plotting (from both fotr and fwvtr)

fotr_data = fotr[col].dropna() if col in fotr else pd.Series()

fwvtr_data = fwvtr[col].dropna() if col in fwvtr else pd.Series()

# Find the most common unit for each column

unit_column = col.replace(text, u)

most_common_unit = "unknown"

if unit_column in fotr:

most_common_unit = fotr[unit_column].value_counts().idxmax()

elif unit_column in fwvtr:

most_common_unit = fwvtr[unit_column].value_counts().idxmax()

# Combine fotr and fwvtr data

combined_col_data = pd.concat([fotr_data, fwvtr_data])

# Apply log transformation

log_combined_col_data = np.log1p(combined_col_data)

# Append data and labels for boxplot

combined_data.append(log_combined_col_data)

labels.append(f"{col.split('_')[0]} ({most_common_unit})")

# Plot a single boxplot for all data

ax.boxplot(combined_data, labels=labels, patch_artist=True,

boxprops=dict(facecolor='skyblue', color='black'),

medianprops=dict(color='red')),

ax.tick_params(axis='both', which='major', labelsize=18)

# Set labels and formatting

# ax.set_ylabel("Log-Transformed Values")

ax.yaxis.set_major_formatter(formatter)

plt.title('Gas Permeability Distributions', fontsize=18)

plt.tight_layout()

plt.show()

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/3840036103.py:28: FutureWarning: The default dtype for empty Series will be 'object' instead of 'float64' in a future version. Specify a dtype explicitly to silence this warning.

fwvtr_data = fwvtr[col].dropna() if col in fwvtr else pd.Series()

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/3840036103.py:27: FutureWarning: The default dtype for empty Series will be 'object' instead of 'float64' in a future version. Specify a dtype explicitly to silence this warning.

fotr_data = fotr[col].dropna() if col in fotr else pd.Series()

# ## transmission rate

dtr['log_WVTR_Updated_Num'] = np.log10(dtr['WVTR_Updated_Num'])

dtr['log_OTR_Updated_Num'] = np.log10(dtr['OTR_Updated_Num'])

fig = px.scatter(

dtr,

x='log_WVTR_Updated_Num',

y='log_OTR_Updated_Num',

color='Type',  # Color by 'Base Material'

symbol='Material',

symbol_sequence= ['circle', 'circle-open'],

hover_data=['Base Material', 'Type', 'Secondary Material'],  # Include additional info in hover

title='Log-scale scatterplot of OTR vs WVTR',

labels={

'log_OP_Updated_Num': 'OTR Updated Num',

'log_WVTr_Updated_Num': 'WVTR Updated Num'

}

)

# Show the plot

fig.show()

plotly.offline.plot(fig, filename='Scatterplot of OTR vs WVTR.html', auto_open=False)

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1347698943.py:2: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

dtr['log_WVTR_Updated_Num'] = np.log10(dtr['WVTR_Updated_Num'])

/var/folders/qs/8x1gpygd3nl0wldh8bphz0f80000gn/T/ipykernel_44813/1347698943.py:3: SettingWithCopyWarning:

A value is trying to be set on a copy of a slice from a DataFrame.

Try using .loc[row_indexer,col_indexer] = value instead

See the caveats in the documentation: https://pandas.pydata.org/pandas-docs/stable/user_guide/indexing.html#returning-a-view-versus-a-copy

dtr['log_OTR_Updated_Num'] = np.log10(dtr['OTR_Updated_Num'])

'Scatterplot of OTR vs WVTR.html'

# Define tick values and labels for power-of-10 formatting

tick_vals_x = np.arange(

int(np.floor(dtr['log_WVTR_Updated_Num'].min())),

int(np.ceil(dtr['log_WVTR_Updated_Num'].max())) + 1

)

tick_text_x = [f"10^{int(i)}" for i in tick_vals_x]

tick_vals_y = np.arange(

int(np.floor(dtr['log_OTR_Updated_Num'].min())),

int(np.ceil(dtr['log_OTR_Updated_Num'].max())) + 1

)

tick_text_y = [f"10^{int(i)}" for i in tick_vals_y]

c = 'Base Material'

# Create the scatter plot

fig = px.scatter(

dtr,

x='log_WVTR_Updated_Num',

y='log_OTR_Updated_Num',

color= c,  # Color by 'Base Material'

symbol='Material',

symbol_sequence= ['circle', 'circle-open'],

hover_data=['Base Material', 'Type', 'Secondary Material'],  # Include additional info in hover

title='Scatterplot of OTR vs WVTR by ' + c + ' under 1atm, 100um',

labels={

'log_WVTR_Updated_Num': 'WVTR Updated Num',

'log_OTR_Updated_Num': 'OTR Updated Num'

}

)

# Update axis labels and ticks for power-of-10 display

fig.update_layout(

xaxis=dict(

title="WVTR Num (g/m2day)",

tickvals=tick_vals_x,

ticktext=tick_text_x,

# type='linear'  # Keeps the axis linear while displaying log ticks

),

yaxis=dict(

title="OTR Num (cm3/m2day)",

tickvals=tick_vals_y,

ticktext=tick_text_y,

# type='linear'  # Keeps the axis linear while displaying log ticks

),

template="plotly_white"

)

# Show the plot

fig.show()

plotly.offline.plot(fig, filename='Scatterplot of OTR vs WVTR (power 10).html', auto_open=False)

'Scatterplot of OTR vs WVTR (power 10).html'

base = dtr['Base Material'].unique()

non_sustainable_materials = ['LDPE', 'HDPE', 'polypropylene', 'polyethylene', 'PET', 'EVOH', 'polyvinyl chloride', 'amylose','polypropylene films']  # Example list

sustainable_materials = set(base) - set(non_sustainable_materials)

Models Fitting

from kneed import KneeLocator

import matplotlib.pyplot as plt

from sklearn.neighbors import NearestNeighbors

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values  # Drop rows with NaN

def plot_k_distance_graph(X, k):

# Fit NearestNeighbors

neigh = NearestNeighbors(n_neighbors=k)

neigh.fit(X)

distances, _ = neigh.kneighbors(X)

# Sort distances for k-th neighbor

distances = np.sort(distances[:, k-1])

# Detect the elbow point

knee_locator = KneeLocator(range(len(distances)), distances, curve="convex", direction="increasing")

elbow_point = knee_locator.knee

epsilon = distances[elbow_point] if elbow_point is not None else None

# Plot the K-distance graph

plt.figure(figsize=(10, 6))

plt.plot(distances, label=f'{k}-th nearest neighbor distance')

if elbow_point is not None:

plt.axvline(x=elbow_point, color='r', linestyle='--', label=f'Elbow point at {elbow_point}')

plt.xlabel('Points')

plt.ylabel(f'{k}-th nearest neighbor distance')

plt.title('K-distance Graph')

plt.legend()

plt.show()

return epsilon

# Plot k-distance graph with elbow detection

epsilon = plot_k_distance_graph(features, k=4)

print(f"Epsilon value detected at: {epsilon}")

Epsilon value detected at: 1.1765824040255133

# check which clusters is the optimium clusters

import matplotlib.pyplot as plt

from sklearn.cluster import KMeans

from sklearn.mixture import GaussianMixture

# Prepare features for clustering

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values  # Drop rows with NaN

# features = features_encoded

# Check for valid data

if features.shape[0] == 0:

raise ValueError("No valid data points available for clustering after removing NaNs.")

from sklearn.metrics import silhouette_score

range_n_clusters = [2, 3, 4, 5, 6, 7, 8, 9, 10]

silhouette_avg_k = []

silhouette_avg_g = []

for num_clusters in range_n_clusters:

# Initialize KMeans and GaussianMixture

kmeans = KMeans(n_clusters=num_clusters, random_state=42)

gmm = GaussianMixture(n_components=num_clusters, random_state=42)

# Fit models

kmeans.fit(features)

cluster_labels_k = kmeans.labels_

cluster_labels_g = gmm.fit_predict(features)  # Use predict for GaussianMixture

# Calculate silhouette scores

silhouette_avg_k.append(silhouette_score(features, cluster_labels_k))

silhouette_avg_g.append(silhouette_score(features, cluster_labels_g))

# Plot silhouette scores for KMeans

plt.figure(figsize=(10, 5))

plt.plot(range_n_clusters, silhouette_avg_k, 'bx-', label='KMeans')

plt.plot(range_n_clusters, silhouette_avg_g, 'ro-', label='GaussianMixture')

plt.xlabel('Number of Clusters (K)')

plt.ylabel('Silhouette Score')

plt.title('Silhouette Analysis for Optimal K')

plt.legend()

plt.show()

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

Kmeans

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values  # Drop rows with NaN

from sklearn.cluster import KMeans

from sklearn.preprocessing import StandardScaler

# Define whether to use normalization

use_normalization = True

# Normalize data if required

if use_normalization:

scaler = StandardScaler()

normalized_features = scaler.fit_transform(features)

else:

normalized_features = features

# Check for valid data

if features.shape[0] == 0:

raise ValueError("No valid data points available for clustering after removing NaNs.")

# Set the number of clusters

k = 6

# Apply KMeans clustering

kmeans = KMeans(n_clusters=k, random_state=42)

labels = kmeans.fit_predict(normalized_features)

# Add cluster labels to the original DataFrame

d_clean = dtr.dropna(subset=['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']).copy()

d_clean['Cluster'] = labels

# Map clusters to Base Material

cluster_base_material_map = (

d_clean.groupby('Cluster')['Base Material']

.apply(lambda x: x.mode()[0] if not x.empty else f"Cluster {x.name}")

.to_dict()

)

# Assign a color palette for clusters

color_palette = px.colors.qualitative.Plotly  # Get Plotly color palette

cluster_colors = {cluster: color_palette[i % len(color_palette)] for i, cluster in enumerate(cluster_base_material_map.keys())}

# Initialize a Plotly figure

fig = go.Figure()

# Add scatter plot for each cluster

for cluster_label in np.unique(labels):

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

cluster_size = len(cluster_data)

# cluster_name = f"Cluster {cluster_label} ({cluster_size} points) - {cluster_base_material_map[cluster_label]}"

cluster_name = f"Cluster {cluster_label} ({cluster_size} points)"

cluster_color = cluster_colors[cluster_label]

marker_colors = [

f"rgba({int(int(cluster_color.lstrip('#')[0:2], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[2:4], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[4:6], 16) * 0.7)}, 1)"

if is_sustainable else cluster_color

for is_sustainable in cluster_data['Material'].str.lower().eq('sustainable')

]

# Adjust marker shape for conventional materials

marker_symbols = [

'triangle-up' if is_conventional else 'circle'

for is_conventional in cluster_data['Material'].str.lower().eq('conventional')

]

fig.add_trace(go.Scatter(

x=cluster_data['log_WVTR_Updated_Num'],

y=cluster_data['log_OTR_Updated_Num'],

mode='markers',

name=cluster_name,  # Legend entry with cluster number and base material

marker=dict(size=10, color=marker_colors, symbol=marker_symbols),

hovertemplate=(

"Base Material: %{text}<br>"

"Type: %{customdata[0]}<br>"

"Secondary Material: %{customdata[1]}<br>"

"Material:%{customdata[2]}<br>"

"log(WVTR): %{x}<br>"

"log(OTR): %{y}"

),

text=cluster_data['Base Material'],

customdata=cluster_data[['Type', 'Secondary Material','Material']].values

))

# Calculate cluster boundary (bounding box)

x_min = cluster_data['log_WVTR_Updated_Num'].min()

x_max = cluster_data['log_WVTR_Updated_Num'].max()

y_min = cluster_data['log_OTR_Updated_Num'].min()

y_max = cluster_data['log_OTR_Updated_Num'].max()

# Convert hex color to rgba for transparency

if cluster_color.startswith("#"):

r, g, b = tuple(int(cluster_color.lstrip("#")[i:i+2], 16) for i in (0, 2, 4))

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = cluster_color  # Fallback if color is not in hex format

# Add a rectangle for the cluster boundary

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=cluster_color, width=3),

fillcolor=fill_color

)

file_suffix = "normalized" if use_normalization else "unnormalized"

fig.update_layout(

title="Kmeans Model Clustering with Cluster Boundaries_log",

xaxis_title="WVTR (g/m2day)",

yaxis_title="OTR (cm3/m2day)",

template="plotly_white"

)

plotly.offline.plot(fig, filename=f'Kmeans_cluster_OP_vs_WVP_log_{file_suffix}.html', auto_open=False)

tick_vals_x = np.linspace(int(d_clean['log_WVTR_Updated_Num'].min()-1), int(d_clean['log_WVTR_Updated_Num'].max()+1), int(d_clean['log_WVTR_Updated_Num'].max()-d_clean['log_WVTR_Updated_Num'].min()+2))

tick_text_x = [f"10<sup>{int(val)}</sup>" for val in tick_vals_x]

tick_vals_y = np.linspace(int(d_clean['log_OTR_Updated_Num'].min()-1), int(d_clean['log_OTR_Updated_Num'].max()+1), int(d_clean['log_OTR_Updated_Num'].max()-d_clean['log_OTR_Updated_Num'].min()+2))

tick_text_y = [f"10<sup>{int(val)}</sup>" for val in tick_vals_y]

fig.update_layout(

title="Kmeans Model Clustering with Cluster Boundaries",

xaxis_title="WVTR (g/m2day)",

yaxis_title="OTR (cm3/m2day)",

template="plotly_white"

)

fig.update_layout(

xaxis=dict(

title="WVTR (g/m2day)",

tickvals=tick_vals_x,

ticktext=tick_text_x,

type='linear',  # Keeps the axis linear while displaying log ticks

tickfont=dict(size=16),

),

yaxis=dict(

title="OTR (cm3/m2day)",

tickvals=tick_vals_y,

ticktext=tick_text_y,

type='linear',  # Keeps the axis linear while displaying log ticks

tickfont=dict(size=16),

),

template="plotly_white"

# Show the updated plot

)

fig.show()

plotly.offline.plot(fig, filename=f'Kmeans_cluster_OP_vs_WVP_{file_suffix}.html', auto_open=False)

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

'Kmeans_cluster_OP_vs_WVP_normalized.html'

cluster_2_data = d_clean[d_clean['Cluster'] == 2]

# Display relevant information

columns_of_interest = ['Base Material', 'Type', 'Secondary Material']

cluster_2_info = cluster_2_data[columns_of_interest]

# Print the details

print(cluster_2_info)

Base Material        Type Secondary Material

57             LDPE  individual               None

58             LDPE  individual               None

59             HDPE  individual               None

68  polylactic acid  individual               None

69  polylactic acid  individual               None

70  polylactic acid  individual               None

Gaussian Mixture Matrix

from sklearn.preprocessing import StandardScaler

from sklearn.mixture import GaussianMixture

# Define whether to use normalization

use_normalization = False

# Select features and drop rows with NaN

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values

# Normalize data if required

if use_normalization:

scaler = StandardScaler()

normalized_features = scaler.fit_transform(features)

else:

normalized_features = features

# Fit the Gaussian Mixture Model

n_components = 6 # Set the number of clusters

gmm = GaussianMixture(n_components=n_components, random_state=42)

gmm.fit(features)

# Predict cluster labels

labels = gmm.predict(normalized_features)

# Add cluster labels to the original DataFrame

d_clean = dtr.dropna(subset=['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']).copy()

d_clean['Cluster'] = labels

# Map clusters to Base Material

cluster_base_material_map = (

d_clean.groupby('Cluster')['Base Material']

.apply(lambda x: x.mode()[0] if not x.empty else f"Cluster {x.name}")

.to_dict()

)

# Assign a color palette for clusters

color_palette = px.colors.qualitative.Plotly  # Get Plotly color palette

cluster_colors = {cluster: color_palette[i % len(color_palette)] for i, cluster in enumerate(cluster_base_material_map.keys())}

# Initialize a Plotly figure

fig = go.Figure()

for cluster_label in np.unique(labels):

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

cluster_size = len(cluster_data)

# cluster_name = f"Cluster {cluster_label} ({cluster_size} points) - {cluster_base_material_map[cluster_label]}"

cluster_name = f"Cluster {cluster_label} ({cluster_size} points)"

cluster_color = cluster_colors[cluster_label]

marker_colors = [

f"rgba({int(int(cluster_color.lstrip('#')[0:2], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[2:4], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[4:6], 16) * 0.7)}, 1)"

if is_sustainable else cluster_color

for is_sustainable in cluster_data['Material'].str.lower().eq('sustainable')

]

# Adjust marker shape for conventional materials

marker_symbols = [

'triangle-up' if is_conventional else 'circle'

for is_conventional in cluster_data['Material'].str.lower().eq('conventional')

]

fig.add_trace(go.Scatter(

x=cluster_data['log_WVTR_Updated_Num'],  # X-axis: log(WVP)

y=cluster_data['log_OTR_Updated_Num'],  # Y-axis: log(OP)

mode='markers',

name=cluster_name,

# symbol = 'Material',

marker=dict(size=10, color=marker_colors, symbol=marker_symbols),

hovertemplate=(

"Base Material: %{text}<br>"

"Type: %{customdata[0]}<br>"

"Secondary Material: %{customdata[1]}<br>"

"log(WVTR): %{x}<br>"

"log(OTR): %{y}"

),

text=cluster_data['Base Material'],

customdata=cluster_data[['Type', 'Secondary Material']].values

))

# Calculate cluster boundary (bounding box)

x_min = cluster_data['log_WVTR_Updated_Num'].min()

x_max = cluster_data['log_WVTR_Updated_Num'].max()

y_min = cluster_data['log_OTR_Updated_Num'].min()

y_max = cluster_data['log_OTR_Updated_Num'].max()

# Convert hex color to rgba for transparency

if cluster_color.startswith("#"):

r, g, b = tuple(int(cluster_color.lstrip("#")[i:i+2], 16) for i in (0, 2, 4))

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = cluster_color  # Fallback if color is not in hex format

# Add a rectangle for the cluster boundary

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=cluster_color, width=2),

fillcolor=fill_color

)

plotly.offline.plot(fig, filename=f'GMM_cluster_OP_vs_WVP_log_{file_suffix}.html', auto_open=False)

tick_vals_x = np.linspace(d_clean['log_WVTR_Updated_Num'].min()-1, d_clean['log_WVTR_Updated_Num'].max()+1, 10)

tick_text_x = [f"10<sup>{int(val)}</sup>" for val in tick_vals_x]

tick_vals_y = np.linspace(d_clean['log_OTR_Updated_Num'].min()-1, d_clean['log_OTR_Updated_Num'].max()+1, 10)

tick_text_y = [f"10<sup>{int(val)}</sup>" for val in tick_vals_y]

# Export the plot

file_suffix = "normalized" if use_normalization else "unnormalized"

# Update layout

fig.update_layout(

title=f"GMM Clustering with Cluster Boundaries_{file_suffix}",

xaxis_title="log WVTR",

yaxis_title="log OTR",

template="plotly_white"

)

# Update axis labels and ticks for power-of-10 display

fig.update_layout(

xaxis=dict(

title="WVTR (g/m2day)",

tickvals=tick_vals_x,

ticktext=tick_text_x,

tickfont=dict(size=16),

type='linear'  # Keeps the axis linear while displaying log ticks

),

yaxis=dict(

title="OTR (cm3/m2day)",

tickvals=tick_vals_y,

ticktext=tick_text_y,

tickfont=dict(size=16),

type='linear'  # Keeps the axis linear while displaying log ticks

),

# template="plotly_white"

)

fig.show()

plotly.offline.plot(fig, filename=f'GMM_cluster_OP_vs_WVP_{file_suffix}.html', auto_open=False)

'GMM_cluster_OP_vs_WVP_unnormalized.html'

DBSCAN

from sklearn.cluster import DBSCAN

from sklearn.preprocessing import StandardScaler

import plotly.express as px

import plotly.graph_objects as go

import numpy as np

# Define whether to use normalization

use_normalization = True

# Select features and drop rows with NaN

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values

# Normalize data if required

if use_normalization:

scaler = StandardScaler()

normalized_features = scaler.fit_transform(features)

else:

normalized_features = features

# Check for valid data

if features.shape[0] == 0:

raise ValueError("No valid data points available for clustering after removing NaNs.")

# ----------------------------------------------------

# 3. Apply DBSCAN clustering

# ----------------------------------------------------

eps = 1.17

min_samples = 4

dbscan = DBSCAN(eps=eps, min_samples=min_samples)

labels = dbscan.fit_predict(normalized_features)

# ----------------------------------------------------

# 4. Add cluster labels to the original DataFrame

# ----------------------------------------------------

# We assume 'd_clean' aligns with 'features' row order

d_clean = dtr.dropna(subset=['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']).copy()

d_clean['Cluster'] = labels

# Optional: map clusters to "Base Material"

cluster_base_material_map = (

d_clean[d_clean['Cluster'] != -1]

.groupby('Cluster')['Base Material']

.apply(lambda x: x.mode()[0] if not x.empty else f"Cluster {x.name}")

.to_dict()

)

# Assign a color palette for clusters

color_palette = px.colors.qualitative.Plotly  # Get Plotly color palette

cluster_colors = {cluster: color_palette[i % len(color_palette)] for i, cluster in enumerate(cluster_base_material_map.keys())}

cluster_colors[-1] = "#d3d3d3"  # Assign a gray color for noise points (Cluster -1)

# ----------------------------------------------------

# 5. Build the Plotly figure

# ----------------------------------------------------

fig = go.Figure()

# Choose a color palette

color_palette = px.colors.qualitative.Plotly

unique_clusters = np.unique(labels)

# ----------------------------------------------------

# 6. Plot each cluster in the original log-space

# ----------------------------------------------------

for cluster_label in np.unique(labels):

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

cluster_size = len(cluster_data)

# cluster_name = f"Cluster {cluster_label} ({cluster_size} points) - {cluster_base_material_map[cluster_label]}"

cluster_name = f"Cluster {cluster_label} ({cluster_size} points)"

cluster_color = cluster_colors[cluster_label]

marker_colors = [

f"rgba({int(int(cluster_color.lstrip('#')[0:2], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[2:4], 16) * 0.7)},"

f"{int(int(cluster_color.lstrip('#')[4:6], 16) * 0.7)}, 1)"

if is_sustainable else cluster_color

for is_sustainable in cluster_data['Material'].str.lower().eq('sustainable')

]

# Adjust marker shape for conventional materials

marker_symbols = [

'triangle-up' if is_conventional else 'circle'

for is_conventional in cluster_data['Material'].str.lower().eq('conventional')

]

fig.add_trace(go.Scatter(

x=cluster_data['log_WVTR_Updated_Num'],

y=cluster_data['log_OTR_Updated_Num'],

mode='markers',

name=f"Cluster: {cluster_name}" if cluster_label != -1 else "Noise",

marker=dict(size=10, color=marker_colors, symbol=marker_symbols),

hovertemplate=(

"Base Material: %{text}<br>"

"Type: %{customdata[0]}<br>"

"Secondary Material: %{customdata[1]}<br>"

"log(WVTR): %{x}<br>"

"log(OTR): %{y}"

),

text=cluster_data['Base Material'],

customdata=cluster_data[['Type', 'Secondary Material']].values

))

# ----------------------------------------------------

# 7. Draw bounding boxes in the correct (original log) domain

# ----------------------------------------------------

# <<< REVISED: bounding boxes must be computed in the same space DBSCAN used,

# and then inverse-transformed to the original log domain (if normalized).

if use_normalization:

# We must inverse-transform for each cluster

for cluster_label in unique_clusters:

if cluster_label == -1:

continue  # skip noise

cluster_indices = np.where(labels == cluster_label)[0]

if len(cluster_indices) == 0:

continue

# Extract normalized points for this cluster

cluster_points_norm = normalized_features[cluster_indices, :]  # shape (k, 2)

# Inverse-transform to get back to [log_OTR, log_WVTR]

cluster_points_orig = scaler.inverse_transform(cluster_points_norm)

# cluster_points_orig[:, 0] => log_OTR

# cluster_points_orig[:, 1] => log_WVTR

# Compute bounding box in the original log domain

x_min = cluster_points_orig[:, 1].min()

x_max = cluster_points_orig[:, 1].max()

y_min = cluster_points_orig[:, 0].min()

y_max = cluster_points_orig[:, 0].max()

# Convert cluster color from hex to RGBA

cluster_color = cluster_colors[cluster_label]

if cluster_color.startswith("#"):

r, g, b = [int(cluster_color.lstrip("#")[i : i+2], 16) for i in (0, 2, 4)]

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = cluster_color

# Add shape

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=cluster_color, width=2),

fillcolor=fill_color

)

else:

# If not normalizing, just use the raw min/max from the data

for cluster_label in unique_clusters:

if cluster_label == -1:

continue

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

if len(cluster_data) == 0:

continue

cluster_color = cluster_colors[cluster_label]

if cluster_color.startswith("#"):

r, g, b = [int(cluster_color.lstrip("#")[i : i+2], 16) for i in (0, 2, 4)]

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = cluster_color

x_min = cluster_data['log_WVTR_Updated_Num'].min()

x_max = cluster_data['log_WVTR_Updated_Num'].max()

y_min = cluster_data['log_OTR_Updated_Num'].min()

y_max = cluster_data['log_OTR_Updated_Num'].max()

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=cluster_color, width=2),

fillcolor=fill_color

)

# ----------------------------------------------------

# 8. Set up integer tick values for the axes

# ----------------------------------------------------

lowest_exponent = -1

# 1. Determine integer exponent ranges based on the data

x_min_int = int(np.floor(d_clean['log_WVTR_Updated_Num'].min()))

x_max_int = int(np.ceil(d_clean['log_WVTR_Updated_Num'].max()))

# Force the minimum exponent to be 0 if it's higher than 0

x_min_int = min(0, x_min_int)

y_min_int = int(np.floor(d_clean['log_OTR_Updated_Num'].min()))

y_max_int = int(np.ceil(d_clean['log_OTR_Updated_Num'].max()))

y_min_int = min(0, y_min_int)

# 2. Create arrays of integer ticks

tick_vals_x = np.arange(lowest_exponent, x_max_int + 1)

tick_vals_y = np.arange(lowest_exponent, y_max_int + 1)

# 3. Generate the text labels as 10^exponent

tick_text_x = [f"10<sup>{val}</sup>" for val in tick_vals_x]

tick_text_y = [f"10<sup>{val}</sup>" for val in tick_vals_y]

# 4. Update axes so they show from 10^0 up to the max exponent

fig.update_xaxes(

title="WVTR (g/m2day)",

tickvals=tick_vals_x,

ticktext=tick_text_x,

range=[lowest_exponent, x_max_int],  # Force axis to span at least from exponent=0

gridcolor='white',

linecolor='grey',

title_font=dict(size=20),   # Increase the x-axis title font size

tickfont=dict(size=16)        # Increase the x-axis tick label font size

)

fig.update_yaxes(

title="OTR (cm3/m2day)",

tickvals=tick_vals_y,

ticktext=tick_text_y,

range=[lowest_exponent, y_max_int],  # Force axis to span at least from exponent=0

gridcolor='white',

linecolor='grey',

title_font=dict(size=20),   # Increase the x-axis title font size

tickfont=dict(size=16)        # Increase the x-axis tick label font size

)

# Update layout title, etc. as usual

file_suffix = "normalized" if use_normalization else "unnormalized"

fig.update_layout(

title= f"DBSCAN Clustering with Cluster Boundaries_{file_suffix}",

template="plotly_white",

plot_bgcolor='white'

)

fig.show()

# Export the plot

plotly.offline.plot(fig, filename=f'DBSCAN_cluster_OP_vs_WVP_{file_suffix}.html', auto_open=False)

'DBSCAN_cluster_OP_vs_WVP_normalized.html'

import numpy as np

import pandas as pd

from sklearn.cluster import DBSCAN

from sklearn.preprocessing import StandardScaler

import plotly.express as px

import plotly.graph_objects as go

import plotly.offline

# -----------------------------

# 1. Prepare Data & Features

# -----------------------------

# (Assuming dtr is your original DataFrame with the columns used below.)

features = dtr[['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']].dropna().values

if features.shape[0] == 0:

raise ValueError("No valid data points available for clustering after removing NaNs.")

use_normalization = True

if use_normalization:

scaler = StandardScaler()

normalized_features = scaler.fit_transform(features)

else:

normalized_features = features

# -----------------------------

# 2. Apply DBSCAN Clustering

# -----------------------------

eps = 1.17

min_samples = 4

dbscan = DBSCAN(eps=eps, min_samples=min_samples)

labels = dbscan.fit_predict(normalized_features)

# -----------------------------

# 3. Add Cluster Labels to DataFrame

# -----------------------------

# We assume that dtr rows align with the features used.

d_clean = dtr.dropna(subset=['log_OTR_Updated_Num', 'log_WVTR_Updated_Num']).copy()

d_clean['Cluster'] = labels

# (Optional) Build a mapping from cluster to a representative Base Material.

cluster_base_material_map = (

d_clean[d_clean['Cluster'] != -1]

.groupby('Cluster')['Base Material']

.apply(lambda x: x.mode()[0] if not x.mode().empty else f"Cluster {x.name}")

.to_dict()

)

# -----------------------------

# 4. Define Helper to Darken Colors

# -----------------------------

def darken_color(hex_color, factor=0.7):

"""Convert hex color to a darkened RGBA string."""

hex_color = hex_color.lstrip('#')

r = int(hex_color[0:2], 16)

g = int(hex_color[2:4], 16)

b = int(hex_color[4:6], 16)

r = int(r * factor)

g = int(g * factor)

b = int(b * factor)

return f"rgba({r}, {g}, {b}, 1)"

# -----------------------------

# 5. Assign Colors to Clusters

# -----------------------------

# Use Plotly's qualitative palette for non-noise clusters.

color_palette = px.colors.qualitative.Plotly

non_noise_clusters = sorted(cluster_base_material_map.keys())

cluster_colors = {cluster: color_palette[i % len(color_palette)]

for i, cluster in enumerate(non_noise_clusters)}

# For noise (cluster -1) assign gray.

cluster_colors[-1] = "#d3d3d3"

# -----------------------------

# 6. Build the Plotly Figure with All Legend Items

# -----------------------------

fig = go.Figure()

unique_clusters = np.unique(labels)

# For each cluster, we separate points by the value in the "Material" column.

# We define three groups:

#   - Sustainable: material equals 'sustainable'

#   - Conventional: material equals 'conventional'

#   - Other: any value besides those two.

for cluster_label in unique_clusters:

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

cluster_size = len(cluster_data)

# Build a name prefix for the legend

if cluster_label == -1:

cluster_name_prefix = "Noise"

else:

# Optionally, you can include the Base Material name in the legend label.

base_mat = cluster_base_material_map.get(cluster_label, "")

cluster_name_prefix = f"Cluster {cluster_label} ({base_mat})"

base_color = cluster_colors.get(cluster_label, "#000000")

# Define masks (using case-insensitive comparisons)

material_lower = cluster_data['Material'].str.lower()

mask_sust = material_lower == 'sustainable'

mask_conv = material_lower == 'conventional'

mask_other = ~(mask_sust | mask_conv)

# --- Sustainable Points (use darkened color and circle marker) ---

sust_data = cluster_data[mask_sust]

if not sust_data.empty:

fig.add_trace(go.Scatter(

x=sust_data['log_WVTR_Updated_Num'],

y=sust_data['log_OTR_Updated_Num'],

mode='markers',

name=f"{cluster_name_prefix} (Sustainable, {len(sust_data)} pts)",

showlegend=True,

marker=dict(

size=10,

color=darken_color(base_color, factor=0.7),

symbol='circle'

),

hovertemplate=(

"Base Material: %{text}<br>" +

"Type: %{customdata[0]}<br>" +

"Secondary Material: %{customdata[1]}<br>" +

"log(WVTR): %{x}<br>" +

"log(OTR): %{y}"

),

text=sust_data['Base Material'],

customdata=sust_data[['Type', 'Secondary Material']].values

))

# --- Conventional Points (use base color and triangle-up marker) ---

conv_data = cluster_data[mask_conv]

if not conv_data.empty:

fig.add_trace(go.Scatter(

x=conv_data['log_WVTR_Updated_Num'],

y=conv_data['log_OTR_Updated_Num'],

mode='markers',

name=f"{cluster_name_prefix} (Conventional, {len(conv_data)} pts)",

showlegend=True,

marker=dict(

size=10,

color=base_color,

symbol='triangle-up'

),

hovertemplate=(

"Base Material: %{text}<br>" +

"Type: %{customdata[0]}<br>" +

"Secondary Material: %{customdata[1]}<br>" +

"log(WVTR): %{x}<br>" +

"log(OTR): %{y}"

),

text=conv_data['Base Material'],

customdata=conv_data[['Type', 'Secondary Material']].values

))

# --- Other Points (use base color and circle marker) ---

other_data = cluster_data[mask_other]

if not other_data.empty:

fig.add_trace(go.Scatter(

x=other_data['log_WVTR_Updated_Num'],

y=other_data['log_OTR_Updated_Num'],

mode='markers',

name=f"{cluster_name_prefix} (Other, {len(other_data)} pts)",

showlegend=True,

marker=dict(

size=10,

color=base_color,

symbol='circle'

),

hovertemplate=(

"Base Material: %{text}<br>" +

"Type: %{customdata[0]}<br>" +

"Secondary Material: %{customdata[1]}<br>" +

"log(WVTR): %{x}<br>" +

"log(OTR): %{y}"

),

text=other_data['Base Material'],

customdata=other_data[['Type', 'Secondary Material']].values

))

# -----------------------------

# 7. Add Bounding Boxes for Each Cluster

# -----------------------------

# Compute bounding boxes in the normalized space and then inverse-transform to the original log domain.

if use_normalization:

for cluster_label in unique_clusters:

if cluster_label == -1:

continue  # Skip noise

cluster_indices = np.where(labels == cluster_label)[0]

if len(cluster_indices) == 0:

continue

cluster_points_norm = normalized_features[cluster_indices, :]  # shape (k, 2)

cluster_points_orig = scaler.inverse_transform(cluster_points_norm)

# Note: columns: [log_OTR_Updated_Num, log_WVTR_Updated_Num]

x_min = cluster_points_orig[:, 1].min()

x_max = cluster_points_orig[:, 1].max()

y_min = cluster_points_orig[:, 0].min()

y_max = cluster_points_orig[:, 0].max()

col = cluster_colors.get(cluster_label, "#000000")

if col.startswith("#"):

r, g, b = [int(col.lstrip("#")[i:i+2], 16) for i in (0, 2, 4)]

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = col

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=col, width=2),

fillcolor=fill_color

)

else:

for cluster_label in unique_clusters:

if cluster_label == -1:

continue

cluster_data = d_clean[d_clean['Cluster'] == cluster_label]

if len(cluster_data) == 0:

continue

col = cluster_colors.get(cluster_label, "#000000")

if col.startswith("#"):

r, g, b = [int(col.lstrip("#")[i:i+2], 16) for i in (0, 2, 4)]

fill_color = f"rgba({r}, {g}, {b}, 0.1)"

else:

fill_color = col

x_min = cluster_data['log_WVTR_Updated_Num'].min()

x_max = cluster_data['log_WVTR_Updated_Num'].max()

y_min = cluster_data['log_OTR_Updated_Num'].min()

y_max = cluster_data['log_OTR_Updated_Num'].max()

fig.add_shape(

type="rect",

x0=x_min, x1=x_max,

y0=y_min, y1=y_max,

line=dict(color=col, width=2),

fillcolor=fill_color

)

# -----------------------------

# 8. Update Axes with Exponential Tick Labels

# -----------------------------

lowest_exponent = -1

x_min_int = int(np.floor(d_clean['log_WVTR_Updated_Num'].min()))

x_max_int = int(np.ceil(d_clean['log_WVTR_Updated_Num'].max()))

x_min_int = min(0, x_min_int)

y_min_int = int(np.floor(d_clean['log_OTR_Updated_Num'].min()))

y_max_int = int(np.ceil(d_clean['log_OTR_Updated_Num'].max()))

y_min_int = min(0, y_min_int)

tick_vals_x = np.arange(lowest_exponent, x_max_int + 1)

tick_vals_y = np.arange(lowest_exponent, y_max_int + 1)

tick_text_x = [f"10<sup>{val}</sup>" for val in tick_vals_x]

tick_text_y = [f"10<sup>{val}</sup>" for val in tick_vals_y]

fig.update_xaxes(

title="WVTR (g/m2day)",

tickvals=tick_vals_x,

ticktext=tick_text_x,

range=[lowest_exponent, x_max_int],

gridcolor='white',

linecolor='grey',

title_font=dict(size=18),   # Increase the x-axis title font size

tickfont=dict(size=18)        # Increase the x-axis tick label font size

)

fig.update_yaxes(

title="OTR (cm3/m2day)",

tickvals=tick_vals_y,

ticktext=tick_text_y,

range=[lowest_exponent, y_max_int],

gridcolor='white',

linecolor='grey',

title_font=dict(size=18),   # Increase the x-axis title font size

tickfont=dict(size=18)        # Increase the x-axis tick label font size

)

# -----------------------------

# 9. Final Layout and Export

# -----------------------------

file_suffix = "normalized" if use_normalization else "unnormalized"

fig.update_layout(

title=f"DBSCAN Clustering with Cluster Boundaries_{file_suffix}",

template="plotly_white"

)

# Disable the legend bar before exporting

fig.update_layout(showlegend=False)

fig.show()

plotly.offline.plot(fig, filename=f'DBSCAN_cluster_OP_vs_WVP_{file_suffix}_no_legend.html', auto_open=False)

'DBSCAN_cluster_OP_vs_WVP_normalized_no_legend.html'

# Exclude noise points (-1) for analysis

clustered_data = d_clean[d_clean['Cluster'] != -1]

# Define helper functions to get unique materials

def list_conventional(x):

return ', '.join(x[x.str.lower() == 'conventional'].unique())

def list_sustainable(x):

return ', '.join(x[x.str.lower() == 'sustainable'].unique())

# --------------------------------------------------------------

# 1) Group by 'Cluster' and calculate the mean & std of log-OTR/WVTR

#    as well as the most frequent materials (and separate material lists).

# --------------------------------------------------------------

cluster_summary = clustered_data.groupby('Cluster').agg({

'log_OTR_Updated_Num': ['mean', 'std'],        # Mean & Std of log(OTR)

'log_WVTR_Updated_Num': ['mean', 'std'],       # Mean & Std of log(WVTR)

'Base Material': lambda x: x.mode()[0] if not x.mode().empty else None,

'Type': lambda x: x.mode()[0] if not x.mode().empty else None,

'Secondary Material': lambda x: x.mode()[0] if not x.mode().empty else None,

'Material': [list_conventional, list_sustainable],

}).reset_index()

# --------------------------------------------------------------

# 2) Flatten the multi-level column names created by agg().

# --------------------------------------------------------------

cluster_summary.columns = [

# 'Cluster' is first

'Cluster',

# log_OTR_Updated_Num

'Mean OTR (log)',

'Std OTR (log)',

# log_WVTR_Updated_Num

'Mean WVTR (log)',

'Std WVTR (log)',

# Base Material, Type, Secondary Material

'Most Common Base Material',

'Most Common Type',

'Most Common Secondary Material',

# Material lists

'Conventional Materials',

'Sustainable Materials'

]

# --------------------------------------------------------------

# 3) Convert mean & std of logs back to original scale (base-10).

#    If your logs are ln-based, switch to np.exp(...) instead.

# --------------------------------------------------------------

cluster_summary['Mean OTR'] = 10 ** cluster_summary['Mean OTR (log)']

cluster_summary['Std OTR']  = 10 ** cluster_summary['Std OTR (log)']

cluster_summary['Mean WVTR'] = 10 ** cluster_summary['Mean WVTR (log)']

cluster_summary['Std WVTR']  = 10 ** cluster_summary['Std WVTR (log)']

# --------------------------------------------------------------

# 4) Display the updated cluster summary

# --------------------------------------------------------------

cluster_summary = cluster_summary.round(3)

print(cluster_summary)

# --------------------------------------------------------------

# 5) (Optional) Save to CSV

# --------------------------------------------------------------

cluster_summary.to_csv('DBSCAN_cluster_summary_with_materials_list.csv', index=False)

Cluster  Mean OTR (log)  Std OTR (log)  Mean WVTR (log)  Std WVTR (log)  \

0        0           0.278          0.108            3.040           0.096

1        1           3.295          0.833            3.004           0.794

2        2           1.102          0.053            5.395           0.145

Most Common Base Material Most Common Type Most Common Secondary Material  \

0              fish gelatin    nanocomposite                montmorillonite

1           polylactic acid       individual                           None

2              carrot puree            blend                            CMC

Conventional Materials Sustainable Materials  Mean OTR  Std OTR   Mean WVTR  \

0                                  sustainable     1.897    1.282    1097.252

1           conventional           sustainable  1970.206    6.806    1008.216

2                                  sustainable    12.635    1.129  248416.313

Std WVTR

0     1.247

1     6.222

2     1.396

# Exclude noise points (-1) for analysis

clustered_data = d_clean[d_clean['Cluster'] != -1].copy()

clustered_data['OTR'] = 10 ** clustered_data['log_OTR_Updated_Num']

clustered_data['WVTR'] = 10 ** clustered_data['log_WVTR_Updated_Num']

# Define the columns you want to keep for each cluster

columns_to_keep = ['Base Material', 'Type', 'Secondary Material', 'OTR', 'WVTR']

# Create a dictionary to store each cluster's DataFrame

cluster_dfs = {}

# Loop over each unique cluster label (excluding noise)

for cluster in clustered_data['Cluster'].unique():

# Create a DataFrame for the current cluster with the selected columns

cluster_df = clustered_data[clustered_data['Cluster'] == cluster][columns_to_keep].reset_index(drop=True)

# Optionally, add a column with the cluster number (if desired)

cluster_df['Cluster'] = cluster

# Store the DataFrame in the dictionary

cluster_dfs[cluster] = cluster_df

# (Optional) Display the DataFrame for each cluster

for cluster, df in cluster_dfs.items():

print(f"\n--- Cluster {cluster} ---")

print(df.head())

filename = f"cluster_{cluster}_data.csv"

df.round(3).to_csv(filename, index=False)

print(f"Cluster {cluster} data saved to {filename}")

--- Cluster 0 ---

Base Material           Type Secondary Material    OTR        WVTR  Cluster

0  fish gelatin     individual               None  4.028  2731.39776        0

1  fish gelatin  nanocomposite    montmorillonite  1.144   709.11288        0

2  fish gelatin  nanocomposite    montmorillonite  1.144   980.50176        0

3  fish gelatin  nanocomposite    montmorillonite  1.144  1199.36376        0

4  fish gelatin  nanocomposite    montmorillonite  1.144  1365.69888        0

Cluster 0 data saved to cluster_0_data.csv

--- Cluster 1 ---

Base Material        Type Secondary Material           OTR         WVTR  \

0             LDPE  individual               None  18948.196512   114.437647

1             LDPE  individual               None  18948.196512    76.163976

2             HDPE  individual               None   4326.464016    19.259856

3  polylactic acid  individual               None    711.301500  2203.925035

4  polylactic acid  individual               None    711.301500  1904.099400

Cluster

0        1

1        1

2        1

3        1

4        1

Cluster 1 data saved to cluster_1_data.csv

--- Cluster 2 ---

Base Material   Type Secondary Material        OTR         WVTR  Cluster

0  carrot puree  blend                CMC  17.745331  580509.5688        2

1  carrot puree  blend                CMC  17.745331  427743.8928        2

2  carrot puree  blend                CMC  17.745331  248977.4112        2

3  carrot puree  blend                CMC  17.745331  202053.3984        2

4  carrot puree  blend                CMC  17.745331  185770.0656        2

Cluster 2 data saved to cluster_2_data.csv

from sklearn.cluster import KMeans, DBSCAN

from sklearn.mixture import GaussianMixture

from sklearn.metrics import silhouette_score, davies_bouldin_score

from sklearn.preprocessing import StandardScaler

import numpy as np

import pandas as pd

# Replace 'data' with your dataset

data = features  # numpy array or pandas DataFrame

# Standardize the data

scaler = StandardScaler()

data = scaler.fit_transform(data)

# Parameters

n_clusters = 6  # Example: number of clusters for K-Means and GMM

eps = 1.17  # DBSCAN parameter

min_samples = 4  # DBSCAN parameter

# Function to count and display cluster sizes

def print_cluster_sizes(labels, algorithm_name):

cluster_counts = pd.Series(labels).value_counts()

print(f"\n{algorithm_name} Cluster Sizes:")

for cluster, count in cluster_counts.items():

cluster_name = "Noise" if cluster == -1 else f"Cluster {cluster}"

print(f"{cluster_name}: {count} data points")

# K-Means

kmeans = KMeans(n_clusters=n_clusters, random_state=42)

kmeans_labels = kmeans.fit_predict(data)

kmeans_silhouette = silhouette_score(data, kmeans_labels)

kmeans_davies_bouldin = davies_bouldin_score(data, kmeans_labels)

print(f"K-Means: Silhouette Score = {kmeans_silhouette}, Davies-Bouldin Index = {kmeans_davies_bouldin}")

print_cluster_sizes(kmeans_labels, "K-Means")

# DBSCAN

dbscan = DBSCAN(eps=eps, min_samples=min_samples)

dbscan_labels = dbscan.fit_predict(data)

# Exclude noise points (-1) for silhouette score

valid_dbscan = dbscan_labels != -1

dbscan_silhouette = silhouette_score(data[valid_dbscan], dbscan_labels[valid_dbscan]) if valid_dbscan.any() else -1

dbscan_davies_bouldin = davies_bouldin_score(data[valid_dbscan], dbscan_labels[valid_dbscan]) if valid_dbscan.any() else float('inf')

print(f"\nDBSCAN: Silhouette Score = {dbscan_silhouette}, Davies-Bouldin Index = {dbscan_davies_bouldin}")

print_cluster_sizes(dbscan_labels, "DBSCAN")

# Gaussian Mixture Model

gmm = GaussianMixture(n_components=n_clusters, random_state=42)

gmm_labels = gmm.fit_predict(data)

gmm_silhouette = silhouette_score(data, gmm_labels)

gmm_davies_bouldin = davies_bouldin_score(data, gmm_labels)

print(f"\nGMM: Silhouette Score = {gmm_silhouette}, Davies-Bouldin Index = {gmm_davies_bouldin}")

print_cluster_sizes(gmm_labels, "GMM")

eva = pd.DataFrame({'Model': ['kmeans', 'dbcsan', 'gmm'], 'Silhouette Score' : [kmeans_silhouette, dbscan_silhouette, gmm_silhouette], 'Davie Bouldin' : [kmeans_davies_bouldin, dbscan_davies_bouldin, gmm_davies_bouldin]})

/Users/windy/opt/anaconda3/lib/python3.8/site-packages/sklearn/cluster/_kmeans.py:870: FutureWarning:

The default value of `n_init` will change from 10 to 'auto' in 1.4. Set the value of `n_init` explicitly to suppress the warning

K-Means: Silhouette Score = 0.9049768895332239, Davies-Bouldin Index = 0.4819257156373331

K-Means Cluster Sizes:

Cluster 1: 180 data points

Cluster 0: 57 data points

Cluster 2: 6 data points

Cluster 4: 6 data points

Cluster 3: 3 data points

Cluster 5: 2 data points

DBSCAN: Silhouette Score = 0.9104179599321588, Davies-Bouldin Index = 0.3737658934703805

DBSCAN Cluster Sizes:

Cluster 2: 180 data points

Cluster 0: 57 data points

Cluster 1: 12 data points

Noise: 5 data points

GMM: Silhouette Score = 0.8988874709560083, Davies-Bouldin Index = 0.4453702034368814

GMM Cluster Sizes:

Cluster 0: 180 data points

Cluster 1: 56 data points

Cluster 3: 10 data points

Cluster 4: 3 data points

Cluster 2: 3 data points

Cluster 5: 2 data points

# Convert data to DataFrame for easy analysis

data_df = pd.DataFrame(data, columns=['OTR', 'WVTR'])  # Replace with your feature names

data_df['Cluster'] = dbscan_labels

# Exclude noise points (-1)

clusters = data_df[data_df['Cluster'] != -1]

# Group by cluster

grouped = clusters.groupby('Cluster')

# Display individual cluster details

print("\nDBSCAN Cluster Details:")

for cluster_id, group in grouped:

print(f"\nCluster {cluster_id}:")

print(f"Number of points: {len(group)}")

print(f"Centroid: {group.mean().values[:-1]}")  # Exclude the 'Cluster' column from mean calculation

print(f"Descriptive Stats:\n{group.describe().drop(columns='Cluster')}")

DBSCAN Cluster Details:

Cluster 0:

Number of points: 57

Centroid: [-0.78159651 -1.49081554]

Descriptive Stats:

OTR       WVTR

count  57.000000  57.000000

mean   -0.781597  -1.490816

std     0.097314   0.086052

min    -0.979563  -1.661053

25%    -0.821547  -1.498152

50%    -0.768027  -1.473580

75%    -0.734070  -1.453280

max    -0.486886  -1.135169

Cluster 1:

Number of points: 12

Centroid: [ 1.93693467 -1.52381671]

Descriptive Stats:

OTR       WVTR

count  12.000000  12.000000

mean    1.936935  -1.523817

std     0.750609   0.712870

min     0.980797  -3.067251

25%     1.398829  -1.549986

50%     1.891496  -1.247357

75%     2.598559  -1.150047

max     2.822907  -0.943656

Cluster 2:

Number of points: 180

Centroid: [-0.0394227   0.62367116]

Descriptive Stats:

OTR        WVTR

count  180.000000  180.000000

mean    -0.039423    0.623671

std      0.047350    0.130097

min     -0.093516    0.437631

25%     -0.062978    0.539380

50%     -0.054438    0.602697

75%     -0.035724    0.679220

max      0.093509    0.954671

eva = eva.round(3)

import seaborn as sns

import matplotlib.pyplot as plt

# Draw the heatmap

plt.figure(figsize=(8, 6))

sns.heatmap(eva, annot=True, fmt=".3f", cmap="coolwarm", cbar_kws={'label': 'Metric Value'})

plt.title("Heatmap of Model Performance Metrics")

plt.ylabel("Model")

plt.show()